## Slide 1
“Time- correlated single photon counting” technique in optical spectroscopy of MgAl2O4
The XIV Annual Scientific Conference of Young Scientists and Specialists “Alushta”
LE THI PHUONG THAO

## Slide 2
Introduction
Figure 1:Schematic illustration structural MgAl2O4 :
Wide band-gap (~9 eV);
High hardness (16 GPa);
Thermal stability (Tmelt = 2135 ˚C);
Low density ~ 3.58 g·cm-3;
High transparent in the visible and infrared wavelength regions;
Excellent radiation resistance.
MgAl2O4
A promising material in optical applications at nuclear power devices, lazer technology and in space.
high thermal stability
radiation resistance
chemical inertness
Magnesium Aluminate spinel
Host for inert matrix fuels in light water reactors
Transmutation target for minor actinides and long life fission products
Diagnostic/optical windows of fusion devices (ITER, DEMO..)
Aerospace engineering
Laser technology
For stoichiometric MgAl2O4:
Mg-Al spinel as a mixed double oxide MgO.nAl2O3
A face-centered cubic structure formed by closely packed oxygen ions.
1/8 (Mg2+) of the tetrahedral sites
1/2 octahedral ones are filled by Al3+ in each unit cell.

## Slide 3
Highly resistant to radiation damage
using fast neutron
Clinard et al, and Tucker et al
using Al and Mg ions
at T of 25-800oC
the damage dose of ~ 100 dpa
Zinkle et al.
Spinel retained crystallinity and exhibited small swelling and amorphization was not observed
Figure 2: C. Kinoshita. Microstructural evolution of Irradiated ceramics
No amorphization

## Slide 4
Swift- heavy ion
(dE / dx )Total = (dE / dx )e + (dE / dx )n
~ 99%
~ 1%
E > 1 MeV/nucleon
High-density electronic excitation
Ion tracks
Amorphization
>100 dpa,
Threshold
SHIs irradiation of spinel:
Information about radiation defects induced by swift heavy ions in spinel has been lacking, especially in the range of high ionization energy losses.
Almost data about radiation damages in spinel was obtained don’t provide information about point defect and its behaviour.
Motivation
Study radiation-induced defects in MgAl2O4 irradiated by swift heavy ions with optical spectroscopy methods _ Photoluminescence and study nature and behaviour of these defects by using Time-collerated single photon counting (TCSPC).
Research gold
Notes: At the same time, irradiated with heavy ion…

## Slide 5
SHIs irradiation parameters
Ions | Energy (MeV) | Se (keV/nm) | Sn (keV/nm) | RP (μm) | Ion fluence (cm-2)
Xe | 152 | 21.040 | 0.099 | 11.46 | 10 10 - 10 13
Figure 3: Schematic imaging of the PL measurements in 152 MeV Xe ion irradiated spinel showing the size of probed volume in comparison with thickness of the whole irradiated layer
Figure 4: Values of electronic and nuclear stopping power were evaluated by SRIM simulation.
A single crystal of stoichiometric MgAl2O4:
Thickness: 500um
IC-100 cyclotron in JINR

## Slide 6
Measurement Setup
Figure 5: Setup for measurement of the photoluminescence kinetics.
1 – Head of the pulse laser,
2 – Photomultiplier Detector Assembly (PMA 175),
3 – Picosecond Diode Laser driver (PDL800-D).
Frequency ~ 1 MHz
Notes: To

## Slide 7
Time-Correlated Single Photon Counting (TCSPC)
Start
Stop
Figure 6: a)Measurement/histogram of start-stop time in time-resolved fluorescence measurement with TCSPC
b) The schematic experimental set-up
Picosecond Pulsed Diode Laser Driver
(PDL 800-D)
TimeHarp 260
a)
b)
Notes: The principle of TCSPC
Thêm hình trong file zalo, giải thích cơ chế theo trong chú thích bên cạnh
high sensitivity, time resolution
The time resolution of this system was about 200ps

## Slide 8
Results
Figure 7: Photoluminescence decay curves from Xe ion irradiated MgAl2O4 (excitation wavelength 445 nm) as function of wavelength (a) and ion fluence (b). IRF – instrumental response function.
Photoluminescence kinetic measurement
Reduction of the decay time with ion influence is due to growing contribution of non-radiative processes that quench the luminescence
The charge-transfer processes between defects or defect-impurity site
In spectral range of 475-660 nm emission wavelength

## Slide 9
Conclusion
The measurements of the photoluminescence decay curves indicated lifetime increases with emission wavelength increasing in spectral range of 475-660 nm and decreases with ion fluence increasing.
It is suggested that reduction of the decay time with ion fluence is due to growing contribution of nonradiative processes that quench the luminescence yield.
The dependence of characteristic lifetimes on registration wavelength is explained by the peculiarities of the charge-transfer processes between defects or defect impurity sites in radiative de-excitation.
Figure 8: Possible mechanisms of the photoluminescence process showing the variation of lifetime with spectral position.

## Slide 10
Thank you
Email: letxi@jinr.ru
lethiphuongthao114@gmail.com

## Slide 11
*Belarusian State University (Minsk, Belarus)
UV (355 nm)
Blue (473 nm)
Green (532 nm)
Registration of the
emission by Peltier-cooled CCD-matrix Andor Technology DU401A-BV
Micro Raman spectrometer Nanofinder High End (LOTIS TII Japan-Belarus)
combined with a 3D scanning confocal microscope

## Slide 12
Basic Principles Behind the TCSPC Electronics
Block diagram of a traditional TCSPC system
CFD = Constant Fraction Discriminator;
TAC = Time to Amplitude Converter;
ADC = Analog to Digital Converter.
Time Harp 260

## Slide 13
Figure : Spectral content of the photoluminescence from single crystalline MgAl2O4 before and after irradiation with 152 MeV Xe ions.
1,9 eV

## Slide 14
Notes: Thedecaycurveswereanalyzed usingEasyTau2software

## Slide 15
E~ 70 – 100 MeV
Modelling the impact of actinide fission fragments
Irradiation
Neutrons
Electrons
Swift heavy
ions
Sample
Anion vacancies
F, F+ and
aggregate
F2, F22+ color centers
Anti-site defects
Al3+׀Mg2+,
Mg2+׀Al3+
Cation
vacancies
V centers