## Slide 1
MAGNETISM AND SUPERCONDUCTIVITY IN PERIODIC AND QUASI-PERIODIC LOW-DIMENSIONAL LAYERED SYSTEMS
61st meeting of the PAC for Condensed Matter Physics,
Dubna, June 26, 2025
Zhaketov V.1,2,3,*,
Zaky A. Zaky E.1,4, Norov D.1,5, Dubkova E.3, Sadradze R.3, Kopytov G.6,
Kolupaev E.D.1,5, Devyaterikov D.I.7, Chernikov A.N.1, Kravtsov E.A.7, Nikitenko Yu.V.1
1 Joint Institute for Nuclear Research, Dubna, Russia
2 Moscow Institute of Physics and Technology, Dolgoprudny, Russia
3 Dubna State University, Dubna, Russia
4 Beni-Suef University, Egypt
5 Lomonosov Moscow State University, Moscow, Russia
6 Tomsk Polithechnic University, Tomsk, Russia
7 M.N. Mikheev Institute of Metal Physics of Ural Branch of RAS, Ekaterinburg, Russia
* zhaketov@nf.jinr.ru

## Slide 2
OUTLINE
Polarized neutron reflectometry
Secondary radiation registration
Enhanced neutron wave field
Periodic supelattice
Fibonacci layered systems

## Slide 3
POLARIZED NEUTRON REFLECTOMETRY
3 / 28

## Slide 4
F
S
Experiment geometry
The determined potential is
the sum for all isotopes
POTENTIAL OF INTERACTION OF NEUTRON WITH MEDIA AT PNR
Possible to use spin-flip signal or products of neutron absobtion to get signal from separate element (isotopes)
But we need
increase signal
4 / 28

## Slide 5
Charged particles (n, α); (n, t); (n, p)
Gamma-quanta (n, γ)
Fission fragments (n, f)
i – isotope, j – type of secondary radiation
Neutron
detector
detector of secondary radiation
sample
REGISTRATION OF SECONDARY RADIATION
Registration of secondary radiation in neutron reflectometry makes it possible to determine the isotopic profiles of elements.
Spin-flip neutrons
Noncoherent scattered neutrons by nuclei
Inelastically scattered neutrons
Diffusely scattered neutrons on medium inhomogeneities
Сharacteristic secondary radiation
Some secondary processes
Aksenov V.L. et al. // Physics of Particles and Nuclei, Vol. 54, No.4, pp. 756-775 (2023)
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 15, no. 3, pp. 549-562 (2021)
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 13, no. 3, pp. 478-487 (2019)
5 / 32
5 / 28

## Slide 6
surface
substrate
i-layer
X
r''
t'
r'
Calculation of each i-layer:
Wave function calculation
each - layer, divide at points, with step
Let us now consider in more detail the calculation of the coefficients , ,
6 / 32
6 / 28

## Slide 7
surface
substrate
i-layer
X
r''
t'
r'
Calculation of
How calculate : set first layer – layer i+1, second i+2 etc., “substrate” – the real substrate of the sample, recurrently calculate the reflection coefficient for such a structure, in the calculations I consider that a neutron falls on the structure from a medium with a potential
1
2
3
…
For each layer:
Further recursive calculation :
- wave-vector at media
- reflection amplitude from layer
- transmission amplitude
where
7 / 32
7 / 28

## Slide 8
Secondary radiation calculation:
6
NEUTRON RESONATORS
n
S
F
V.L. Aksenov et al. // Physica B 276-278 (2000) 946-947.
Possible strong
signal enhancement
8 / 32
8 / 28

## Slide 9
RESONANCE NEUTRON REFLECTOMETRY FOR HYDROGEN DETECTION (THROUGH SPIN-FLIP)
L. Guasco, Yu.N. Khaydukov, S. Pütter, L. Silvi, M.A. Paulin, T. Keller, B. Keimer // Nature Communications, Vol. 13, No. 1, pp. 1-8 (2022)
Middle of the structure
Surface of the structure
On substrate
Secondary radiation
Secondary radiation
Secondary radiation

## Slide 10
A gamma radiation signal was obtained from an ultrathin (1 nm) layer of gadolinium placed in a neutron resonator. The mass of gadolinium used in the experiment (3 micrograms) is 25 times less than in the previous experiment (Zhang et al., PRL 72 (1994)).
The work was performed on the REMUR spectrometer (IBR-2, Dubna) in collaboration with colleagues from JINR (Dubna), IPM RAS (Yekaterinburg), and MPI FKF (Stuttgart)
GAMMA RADIATION SIGNAL FROM AN ULTRATHIN LAYER OF GADOLINIUM
Khaydukov Yu.N. et al. // Physics of Particles and Nuclei Letters, Vol. 21, No. 5, pp. 1065-1068 (2024)
10 / 28

## Slide 11
Structures Nb(25nm)/Gd(df)/Nb(25nm) were investigated
Observed reducing of Tc with increasing of magnetic moment
Superconducting coherent length in gadolinium
Dependance
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
EFFECT OF MAGNETISM ON SUPERCONDUCTIVITY IN NB/GD/NB TRILAYERS
Q(nm-1)
11 / 28

## Slide 12
Fe
SLD
Cr
Fe
Cr
Si substrate
Fe
Cr
}
Bilayer thickness d
d = 32.8 Å + 30 Å = 62.8 Å
Total: 20 bilayers
•••
PERIODIC SUPERLATTICES
Wolfe-Bragg Law :
Bragg peaks
Keising
oscillations
12 / 28

## Slide 13
Results of experimental data fitting
Khaydukov Yu.N. et al. // Phys. Rev. B, 99, 140503 (2019)
Al2O3
Nb(25nm)
Gd()
x 12
Periodic superlattices – artificial crystals with
Decreasing of the magnetic moment of the structure [Nb(25 nm)/Gd(x=1.2, 3, 5 nm)]х12 below
Transition of a ferromagnetic structure into a superconducting state (artificial magnetic superconductor)
DIAMAGNETISM OF PERIODIC FERROMAGNETIC-SUPERCONDUCTING STRUCTURE
>
13 / 28

## Slide 14
2018
Recently, a new proximity effect has been described in ferromagnetic-superconducting layered nanostructures, which is characterized by a large scale (10 nm) of the interaction of superconductivity and magnetism, and which takes place for any ferromagnets.
2022
Giant electromagnetic proximity effect in
superconductor/ferromagnet superlattices
A.V. Putilov, S.V. Mironov, A.S. Mel’nikov, A.I. Buzdin
ELECTROMAGNETIC PROXIMITY EFFECT
Appl. Phys. Lett. 113, 022601 (2018)
Phys. Rev. B 105, 064510

## Slide 15
Investigated structures:
1) Dy (2000 Å) 2) Ho (2000 Å) 3) [Dy (60 Å)/Ho (60 Å)]×34
Dy
Ho
FURTHER PERSPECTIVE – RARE EARTH METALS DYSPROSIUM AND HOLMIUM
Devyaterikov D.I. et al. // Journal of Surface Investigations, Vol. 16, No. 5, pp. 839-842 (2022)
Devyaterikov D.I. et al. // Physics of Metals and Metallography, Vol. 122, No. 5, pp. 465-471 (2021)
Systems with nontrivial magnetic ordering are promising for studies of proximity effects, since they have low phase transition temperatures
Dy (2000 Å)
T=
Dy (2000 Å)
T=
[Dy (60 Å)/Ho (60 Å)]×34
Dy
Ho
15 / 28

## Slide 16
R++ for an incoherent fan
R++ for an incoherent spiral
R++ for coherent spiral (6 layers)
R++ for coherent fan
Dy / Ho 60A
z
Mz
NEUTRON REFLECTIVITY FOR HELICOID

## Slide 17
EXPERIMENT AT CSNS
Proposal # P0224072800043 at CSNS. 18-22 December 2024
Samples: Al2O3 // [Nb(250Å)/RE(dF)]x12/ Nb(50Å), RE=Dy,Ho, dF =2,4,6 nm
17 / 28

## Slide 18
QUASICRYSTAL
Long range order
Periodicity
Long range order
Periodicity
Long range order
Periodicity
CRYSTAL
DISORDERED MEDIA
→ Quasicrystals are non-periodic but deterministic
→ Quasicrystals have long-range order and Bragg diffraction is possible
(Penrouz mosaic)
Vekilov Yu.Kh., Chernikov M.A. Quasicrystals //
// Physics–Uspekhi, volume 180, no. 6 (2010).
Electron diffraction patterns of the icosahedral phase Al69.5Pd21Mn9.5:
(a) along the axis of symmetry of the second order,
(b) along the third order symmetry axis,
18 / 28

## Slide 19
LAYERED QUASIPERIODIC SYSTEMS (FIBONACCI)
A
B
Periodic structure:
BABABABABABA…
Quasiperiodic structure:
BABBABABBABBABABBABAB
Disordered structure:
BBBABABAABAAA
The figure shows: the quasiperiodic structure obtained for the Fibonacci series member ; periodic structure; and an disordered structure obtained using a random number generator.
,
,
,
,
,
,
,
BABBABABBABBABABBABAB
– number of layers,
– spatial position of layers,
– wave-vector.
This talk about system like one-dimentional Penrose mosaic
19 / 28

## Slide 20
PHOTOLUMICESCENCE AT PHOTONIC CRYSTAL
Z. Valy Vardeny et al. // Nature Photonics, Vol. 7, pp. 177-187 (2013)
Razdolski, T. Murzina, O. Aktsipetrov et al . // arXiv:0902.2644v1
P. Vinogradov, Yu. E. Lozovik, A. M. Merzlikin. // PHYSICAL REVIEW B 80, 235106, 2009

## Slide 21
MODELING OF TECHNICAL ERRORS DURING SPUTTERING
thickness deviations
skip random layer
roughness
Конформные шероховатости
Некореллированные шероховатости

## Slide 22
Work describes the observation of a superconducting transition in a bulk Al-Zn-Mg quasicrystal at a temperature Tc<0.05 K. Thus, the authors showed the possibility of the existence of superconducting correlations in quasi-ordered systems, and called this type of superconductivity “fractal”.
SUPERCONDUCTIVITY OF QUASICRYSTALS
Kamiya K. et al. // Nature Communications, 9:154 (2018)
Shiro Sakai, Nayuta Takemori, Akihisa Koga, and Ryotaro Arita //
PHYSICAL REVIEW B 95, 024509 (2017)

## Slide 23
Ryuji Tamura et al. // J. Am. Chem. Soc. 2021, 143, 19938−19944
FAR MAGNETIC ORDERING AT QUASICRYSTALS
Speaking about the magnetic behavior in a number of quasicrystals, a spin glass state was observed, but in it was shown that “exotic” long-range magnetic order is possible in Au–Ga–Gd and Au–Ga–Tb quasicrystals. At the same time, the characteristic Curie temperatures for these materials are relatively low TCurie<25 K.

## Slide 24
NEUTRON REFLECTIVITY FOR QUASIPERIODIC LAYERED SYSTEM
In figure shown calculations of the neutron reflectivity for a layered quasiperiodic structure of the Gd(2 nm)/Nb(25 nm) type; a similar periodic system was studied in [7]. Calculated dependencies for various Fibonacci orders are shown. The thickness of the ferromagnetic layer is equal to half the correlation length of superconductivity in gadolinium . The grazing angle of the neutron beam on the sample is 5 mrad. Magnetic induction in this calculation was assumed to be zero. In the calculations, it was assumed that the structure was deposited on a sapphire substrate. It can be seen that the neutron reflectivity ceases to change, starting from the Fibonacci order F10.
In figure shown the neutron reflectivity for quasiperiodic, periodic and disordered layered structures. The calculation is given for a layered structure of the Gd(2 nm)/Nb(25 nm) type. A calculation is presented for a quasiperiodic structure of the Fibonacci order F9; this structure is characterized by 34 layers of Gd, which is the optimal value for deposition of the structure. The calculations took into account that the total thickness of gadolinium and niobium was the same for all three types of structures. It is shown that for a disordered structure no equidistant peaks are observed, while characteristic Bragg peaks for a periodic structure are visible. For a quasi-periodic structure, more pronounced “quasi-Bragg” peaks are observed.
24 / 28
Fibonacci order
Square under peak
Quasicrystall
Periodic structure
Random

## Slide 25
Sample 25х25х2 mm3
Vector magnet, HTSC
built-in liquefier of
helium-3 and helium-4,
2.2 К – final temperature
Cryocooler, 2 pulse tubes,
0.8 W at 4.2 К
1-main flange; 5,6,11,12,13,14 -heat exchangers; 15 – throttle, 18- activated carbon; T1,T2 – thermistors
A.N. Chernikov / REFRIGERATOR 3Hе BASED ON CLOSED CYCLE CRYOCOOLER COOLING// CONDENSED MATTER RESEARCH AT THE IBR-2, International conference, Dubna, April 25-29, 2022, Abstract book, p.47- 48
3He refrigerator (0.5k), or a 3He dilution refrigerator in 4He (50 mK), with a vertical shaft with a diameter of 30 mm to load the sample
g- detector
nx
Y
By 0-3 T
Bx 0-1 T
@ A.N. Chernikov
CRYOSTATE WITH HTSC MAGNET FOR REMUR REFLECTOMETER
Altynov A.V. et al. // Journal of Surface Investigation, Vol.18, No.4, pp. 900-907 (2024)
25 / 28

## Slide 26
RF MAGNETIC FIELD MODULE
The first working prototype for reflectometric studies in static and oscillating magnetic fields was manufactured and installed
The first demonstration TOF spectra of neutron reflection in static and oscillating fields for a simple ferromagnetic sample were obtained
Protection was improved, the influence of the parasitic neutron beam was significantly reduced (fast neutrons, direct visibility to the AZ)
New spin-flipper drivers manufactured by PNPI were connected
The detector's electromagnetic protection from interference was improved
The cooling of the electromagnet was modernized
Data for new module
Influence of RF magnetic field
coil
spin
+
-
++, --
-+
+-
the parasitic neutron beam
was significantly reduced
2D spectra with RF field
for PN polarization

## Slide 27
CONCLUSION
The mode of recording secondary radiation at PNR realized: charged particles, gamma quanta and neutrons with spin flip, which allows determining the spatial profile of individual isotopes. Resolution and less.
Superconductivity affects magnetism in layered systems, recent works relate to the possibility of superconductivity influencing a spiral helimagnet.
It is proposed to study Fibonacci layered systems, which is due, firstly, to methodological interest, and secondly, to the problems of superconductivity and magnetism, dynamics of light atoms.
27 / 28

## Slide 28
THANK YOU FOR YOUR ATTENTION !