## Slide 1
90 years of Raman effect:
surface-enhanced micro-CARS mapping of organic molecules
Grigory Arzumanyan
FLNP, Sector of Raman spectroscopy
48th meeting of the PAC for Condensed Matter Physics
14 – 15 June 2018

## Slide 2
2
2
OUTLINE
Foreword
90-years of Raman effect: history in brief and key milestones
3. Current results on surface-enhanced coherent
antistokes raman scattering (SECARS).
4. Summary

## Slide 3
Science is united
“You can not draw a line between large and small, as both are equally important for a single whole”
Niels Bohr
Discovery of the Raman effect – 1928, Nobel prize, 1930
Discovery of the neutron by James Chadwick – 1932, Nobel prize, 1935

## Slide 4
4
90 YEARS of RAMAN EFFECT
The effect was predicted theoretically by Adolf Smekal in 1923
Discovered by C.V. Raman and K.S. Krishnan (student of C.V. Raman) in liquids (Calcutta, 28 Feb., 1928),
and independently by
G.S. Landsberg and L.I. Mandelstam in crystals (Moscow, MSU, 21 Feb., 1928)
C.V. Raman
G.S. Landsberg
L.I. Mandelstam
A. Smekal
C.V. Raman – Nobel Prize in Physics, 1930

## Slide 5
Scattering of light by molecules
Diagram of the Rayleigh and Raman Scattering Processes
Raman is based on the inelastic scattering of incident radiation on molecular vibrations/rotations

## Slide 6
Historical photos of discovery (1928)
Raman - Krishnan
scattering spectrum,
benzene
incident light
scattering spectrum,
quarts seal (rhinestone)
Landsberg - Mandelstam

## Slide 7
The main specificity distinguishing Raman/IR spectroscopy from other spectroscopic methods – both of them are molecular vibrational spectroscopy
Raman scattering is also known as a “fingerprint spectroscopy”
7
Although the spectral features of Raman and infrared spectra can be interpreted in a similar way the selection rules are different.
Infrared absorption is sensitive to the change of the dipole moment µ during the vibration.
A Raman active vibration is sensitive to the change of polarizability during the vibration.

## Slide 8
8
Classical Raman Physics
Polarizability induced dipole equation
Scattering at the combination frequencies (Raman effect)

## Slide 9
Raman scattering is weak:
1 in 106 incident photons are Raman scattered
9
Raman signal is very informative – vibrational frequencies are characteristic of chemical bonds (chemical structure) in a specific molecule: normal modes

## Slide 10
90-years of Raman effect: key milestones
10
1961 – invention of lasers, a new generation of light excitation sources – Nobel Prize in Physics (1964), A.M. Basov, A.M. Prokhorov, C.H. Townes
1966 – CARS: Coherent Anti-Stokes Raman Scattering,
first recordings by P. D. Maker and R. W. Terhune, Ford Motor company
1974 – SERS: Surface-Enhanced Raman Scattering, first demonstration by M. Fleischmann – a technique which provides many orders of magnitude increases in Raman intensity
1985 – TERS (or nano-Raman): Tip-Enhanced Raman Scattering - the concept was first proposed by Wessel in 1985, and was experimentally realized in 2000 (nanoscale resolution imaging)
From the 80s to the present: improvement of the optics, filters (especially notch filters) , detectors (PMT, CCD), soft, etc.
Modern trends:
combination of CARS with SERS – SECARS
Shell-Isolated NP Enhanced Raman Spectroscopy – SHINERS

## Slide 11: Surface Enhanced micro-CARS from Gold Nanoparticle-Immobilized Organic Molecules at a Nanostructured CeO2/Al Film
SECARS
11

## Slide 12
Raman
Multimodal optical platform at JINR
12
Second harmonic &
sum frequency
generation
F-CARS, E-CARS, P-CARS
SERS
SECARS
SHG, SONICC
Transmitted and reflected channels
Up-conversion luminescence
“CARS” microscope

## Slide 13
ωvib = ωpump - ωStokes
CARS is a third-order nonlinear process that involves a pump beam at a frequency ωp and a Stokes beam at a frequency of ωs. The signal at the anti-Stokes frequency of ωas = 2ωp- ωs is generated in the phase-matching direction.
The sample is stimulated through a four-wave mixing parametric process.
The vibrational contrast in CARS is created when the pump-Stokes frequency difference matches molecular vibration of a particular chemical bond  = ωvib and the oscillations of molecules with that bond are driven coherently. Thus, CARS provides a chemically specific signature of various molecules.
Physical background of CARS
ICARS(ω) ~ |CARS(3)|2 x Ip2 IS x N2
(3) – third-order nonlinear susceptibility

## Slide 14
The CARS process in details
CARS energy diagram
a
b
c
d
Non-resonant component arises from
the electronic contributions to (3) : a) off-resonance transitions, b) two-photon non-resonant contribution.
ωAS = 2ωp- ωSt
(3) – third-order nonlinear susceptibility
ICARS(ω) ~ |CARS(3)|2 x Ip2 IS x N2
CARS microscopy is a coherent imaging method
in which the induced polarization assumes a
well-defined phase relation with the excitation fields.
Notes: Fig.a Step 1: Shine (intense) light onto the molecules to create (many) virtual states. This light will pump many molecules and is called the pump beam (ωP).
+
Step 2: Shine (intense) light onto the molecules with appropriate energy to “to stimulate the depopulation” of the virtual state. This energy is the Stokes energy (less than excitation). Hence, the light is the Stokes beam (ωS).
Fig.b The consequence of this double illumination is the dense population of a vibrational sub-state of the ground state, which is very specific to the chemical properties. The selection is tuned by the tunable pump beam.
Fig.c In order to visualize the populated vibrational state, we use the pump beam as a probe to elevate the molecule to a new virtual state. (No action needed, light is still on).
Fig.d The molecules will relax from this virtual state to the ground state, the energy is now larger than the pump, consequently “bluer” than the pump and hence called “anti-Stokes”. This is the detected signal.
In CARS microscopy, the electronic contributions to (3) are exhibited as a nonresonant background signal with no vibrational contrast and need to be minimized. By taking advantage of the Raman depolarization ratio of certain modes, thr resonant signal can be separated from the nonresonant background when polarization sensitive detection is employed. P-CARS significantly enhances the image quality and contrast.

## Slide 15
15
Оptical layout of SECARS experiments
SECARS
SECARS
SECARS
Nikon TE2000S
H7844, Hamamatsu
Fast mapping
HS 101H, PROSCAN, Belarus
Slow mapping
Fast mapping
Slow mapping

## Slide 16
Analyte/reporter molecules
Al/CeO2/AuNP/DTNB 1900 nm-thick film
Al/CeO2/AuNP/mPBA 1900 nm-thick film
mercaptoPhenylBoronic acid (mPBA)
Dithionitrobenzoic acid (DTNB)
16

## Slide 17
17
SERS-active substrates*: Al/CeO2/AuNP
Microphotography
29×29 μm
SEM images of a CeO2/Al/Al2O3 sample surface with the TNB-modified Au‐NPs:
(a) ~7.5 µm × 4.5 µm , (b) ~0.6 µm × 0.4 µm
0.5 mm thick
* [1] I. Kurochkin, I. Ryzhikov, A. Lagarkov, et al//Advanced Electromagnetics 2014, 3, 57
[2] I. N. Kurochkin, I. A. Ryzhikov, A. N. Lagarkov, et al//MSU Chem. Bull. 2015, 70, 102

## Slide 18
Preliminary to SECARS
test-control measurements
18

## Slide 19: SERS spectra from: Al/CeO2/Au/DTNB и Al/CeO2/Au/MPBA 633 nm laser excitation
SERS (DTNB)
SERS (MPBA)
SERS spectrum of DTNB is dominated by the strong peaks at 1338cm−1 and 1555cm-1 assigned as the symmetric stretch of the nitro group s(NO2) and the aromatic ring stretch, respectively.
SERS spectrum of MPBA is dominated by the strong bands at 1073cm-1 and 1585cm-1 assigned to the in-plane bending and stretching modes CCC+CS and CC, respectively.
19

## Slide 20: Comparison of the spatial distribution of DTNB 1338 см-1 and 1555 см-1 lines intensities, and 450 см-1 CeO2 Excitation: 532 nm
SERS substrate
CeO2
DTNB
DTNB
Scan area: 23 х 18 µm
1555 cm-1
1338 cm-1
Camera
450 cm-1
20

## Slide 21: Definition of optical damage threshold of the sample
Safe operation: IL<200-300 kW/cm2
(or 2-3mW/µm2)
~ 6x1015 photons/µm2/s
21
1338 cm-1
450 cm-1

## Slide 22
Direct SECARS measurements
22

## Slide 23
23
Spatial distribution of epi-CARS (epi-TCFWM) signal for unmodified Au-NPs on CeO2 film surface
λp = 932 nm (1338 cm-1)
TNB resonance line
(λaS = 828 nm)
λp = 900 nm (1714 cm-1)
Nonresonance
CARS laser powers: Pp ≈ 30 µW и PS ≈ 52 µW
40 µm × 40 µm, 51 х 51 pixels, slow mapping with step ~ 0.8 µm
The numbers in the look-up tables (LUT) correspond to ADC counts
(λaS = 780 nm)
SECARS imaging contrast of signal-generating Au-NP structures lies in the range of 250-700, normalized by the product P2p × PS are ~ 0.15–0.87 counts/µW3 (relation ~ 6).
23

## Slide 24
Highly-contrast SECARS resonant micro-image of a sample surface area modified with TNB/Au-NPs conjugates
24
Scan area: 24 х 24 µm, resolution: 251 х 251 pl
λp = 932 nm (≈300 µW), λS = 1,064 nm (≈1,000 µW), λaS = 828 nm
fast-mapping, step 0.1 µm, 1s/image
Background signal ~ 45 counts
1338cm-1
Contrast of the SECARS image of TNB/Au-NPs ~ 400

## Slide 25: SECARS resonant image of a sample surface area modified by CeO2/Al/Al2O3/Au-NP/mPBA
19.3×19.3 µm, 20×20 pl
λp = 912 nm (≈900 µW), λS = 1064 nm (≈1200 µW)
λaS ≈ 798 nm
Slow scan with a step of 1.0 µm, 1s/pl
Background signal ~ 25 counts
25
Imaging contrast is ~ 50 ,
Normalized by the product P2p × PS is ~ 1.3·10-6 counts/ µW3
1571 сm-1

## Slide 26: Comparison/correlation of SECARS и SERS signals distribution from CeO2/Au-NP/mPBA
Scan area 29×29 µm, slow mapping with a step of 1 µm, 1s/pl
SERS: 785nm, 1 mW, 1571 сm-1 - 4·1015 photons/µ2/s, (λS = 895 nm)
CARS: λp = 912 nm (1571cm-1), 0.3 mW (λp) +1.2 мВт (λS) – totally ~ 8·1015 photons/µ2/s
26
SERS, 1571 сm-1
SECARS, 1571 сm-1
Imaging contrasts ~ 50 (SECARS) и 7 (SERS)

## Slide 27: Comparison/correlation of SECARS и SERS signals distribution from CeO2/Au-NP/mPBA in 3D performance
SERS
SECARS
27

## Slide 28
28
Resonant and nonresonant SECARS micro-images of TNB/Au-NPs on CeO2 film surface
Resonance
λp = 932 nm
(1338 cm-1)
Nonresonance
λp = 900 nm
(1714 cm-1)
40 × 40 µm
51 х 51 pl
Pp ≈ 30 µW
PS ≈ 52 µW
Resonance
Counts ~ 6000
Backgr. ~ 25
Contrast ~ 240
(Norm. 0.13)
Nonresonance
Counts ~ 160
Backgr. ~ 5
Contrast ~ 30
(Norm. 3.6х10-3)
resonance/nonresonance ratio:
≈ 35 with TNB modified molecules
≈ 6 without TNB

## Slide 29
SUMMARY
The very first experiments on SECARS mapping have been done in Russia, FLNP, JINR.
Nonlinear CARS microscopy is an efficient and fast technique for imaging with much stronger signal and chemical contrast without using tags.
The excellent chemical imaging contrast and ultrasensitive detectability of the reporter molecules can be achieved by SECARS.
29
Results are published in JRS (IF ~ 3.0)
G. Arzumanyan, K. Mamtkulov, V. Fabelinsky, V. Smirnov, et al// JRS, 2018, 1-10, https://doi.org/10.1002/jrs.5333
and
recently presented (G. Arzumanyan) at the jubilee conference dedicated to the 90-years of the Raman effect in Novosibirsk, 27 May – 01 June 2018

## Slide 30
30
Thank You!

## Slide 31
31
“CARS” microscope parameters

## Slide 32
Tip Enhanced Raman Scattering (TERS) or nano-Raman –
brings Raman spectroscopy into nanoscale resolution imaging
TERS imaging is performed with an AFM-Raman spectrometer, a SPM integrated with an optical micro-spectrometer.
TERS combines the chemical sensitivity of surface-enhanced Raman spectroscopy (SERS) with high spatial resolution of scanning probe microscopy (SPM) and enables chemical imaging of surfaces at the nanometer length-scale.
TERS image of single wall carbon nanotubes with spatial resolution of ~ 30 nm
32
TERS signals are not strong enough because
there is only one tip working as a signal amplifier.

## Slide 33
33
SHINERS – a new generation of Raman technique
Shell-Isolated Nanoparticle Enhanced Raman Spectroscopy
Au or Ag NPs are employed with a layer of ultrathin inert silica shell.
Each Au core-inert shell nanoparticle can be considered as a TERS tip.
Under a laser spot, the shell-isolated nanoparticles monolayer is equal to thousands of tips, thus the obtained Raman signal is very strong.
The ultrathin shell is used to avoid the direct contact of molecules with Au or Ag NPs, thus the obtained signal is just from the interested species adsorbed on the substrate.