## Slide 1
Fabrication of semiconductors using SiNPs synthesized from SiO2 extracted from agricultural waste
Ntombizonke Kheswa

## Slide 2
RBS/ERDA
NMP/RBS
3 MV Tandetron Accelerator Layout
Nanoprobe

## Slide 3
Research themes
Tandetron Laboratory: Research Focus

## Slide 4
Layout of the 6 MV Tandem Accelerator

## Slide 5
Accelerator Mass Spectrometry (AMS),
Materials engineering and research using Ion Beam Analysis (IBA) techniques,
Ion Implantation,
Environmental Radioactivity,
Stable light isotope analyses, and
Low energy Nuclear Physics.
TAMS Laboratory: Research Focus

## Slide 6: Renewable materials research
Agricultural waste to:
Extract SiO2 and thermal-reduction to Si
Use this to make value added materials like:
Dye-sensitised solar cells
Perovskite solar cells
Make Biochar to use as anodes
Magnetic semiconductors for spintronics

## Slide 7: Synthesis of SiO2NPs from SCBA

## Slide 8: PIXE analysis of SCBA

## Slide 9: SiNPs

## Slide 10: Thin film deposition for n-p type cell fabrication
EBEAM vacuum evaporation systems was used to deposit thin film solar cells.
Substrate-ITO
Si n-type layer was created by depositing bismuth on Si.
Si p-type lay was created by depositing boron on Si layer
Ag deposited as a contact layer
The thicknesses were verified using AFM and RBS

## Slide 11: Dye Sensitised Solar Cell
General design
Our construction
TCO- ITO
SiNPs thin film made by EBEAM
Electrolyte –KI
Dye-metallic dye
Counter electrode-polymer

## Slide 12: cell performance testing
DSSC
P-n type Si SC

## Slide 13: Projects in the pipeline
Perovskite cells and magnetic semiconductors using SiNPs from biomass conversion.
Notes: 111

## Slide 14: Thank you for your attention. Ngiyabonga!