## Slide 1
Sergey Vinogradov
P.N. Lebedev Physical Institute of the Russian Academy of Sciences
Development of a measurement methodology
for the excess noise factor of avalanche multiplication below breakdown for APD, LGAD, SiPM

## Slide 2
Pixel detector => Monolithic Active Pixel Sensors (MAPS)
  high granularity ~ 50 um
  low scattering – low material budget
  on-chip ROIC
Timing detector => Low Gain APD (LGAD)
  time resolution ~ 10 – 30 ps
  low granularity ~ 1 - 2 mm
4D tracking detector: MAPS + LGAD => Monolithic LGAD
Avalanche multiplication trade-off: Gain vs Excess Noise Factor (ENF)
  No studies on ENF of LGAD except [1]
  [1] Bertuccio, et al. (2024). Current Noise Spectral Density and Excess Noise of a Silicon Low-Gain Avalanche Diode (LGAD). IEEE Trans. Electron Devices, 71(10), 5845–5851.
  No studies on ENF of SiPM below breakdown (avalanche with negative feedback)
      LPI basic studies of ANF APD (1980s – 1990s)
  No studies on ENF of TAPD below breakdown (deep spherical junction SiPM)
      TAPD + MAPS concept reported on SPD meetings 2023, 2024
      Time resolution ~ energy resolution ~ ENF [2]
        [2] Vinogradov, S. (2015). Analytical model of SiPM time resolution and order statistics with crosstalk. Nuclear Instruments and Methods in Physics Research A, 787, 229–233.
Motivation to study avalanche noise

## Slide 3
Mei Zhao, LGAD sensor development : From ATLAS high granularity timing detector to future collider, CEPC International Workshop 2024.
MAPS + LGAD => Monolithic LGAD
ЦЕРН, проект PicoLGAD: матрица пикселей размером 65 мкм, 2022 г.
IHEP, проект AC coupled Strip LGAD: разрешение около 15 мкм, 2024 г.

## Slide 4
S. Vinogradov, On possible development of MAPS based on spherical p-n junction, SPD collaboration meeting 2024, 2023.
Sensor and FEE are isolated and independent
All front-side area is available for FEE
High efficiency with lowest capacitance
High radiation hardness is demonstrated
MAPS + TAPD (R&D by LPI + MIET)

## Slide 5: Excess noise factor (ENF) = measure of noisiness of multipliers and amplifiers
ENF in multipliers (APD, PMT, SiPM):
ENF in amplifiers:
Noise factor (F) measures degradation of the signal-to-noise ratio (SNR), caused by components in a signal chain.
High ENF
Low ENF
1 electron → M electrons

## Slide 6: Main APD trade-off: Gain vs Excess Noise Factor
Excess noise of avalanche multiplication => Gain ~ ENF @ Gain > 10; Max Gain ~ 30
σGain
δ(1)
Gain
L. Yan et al. Appl. Phys. Lett. 111, 101104 (2017)
Gain = FWHM = 2.35 σGain
=>
ENF ≤ 1.18 to resolve 1 phe
Conradi, J. IEEE Trans. ED, 19(6), 713 (1972)

## Slide 7: Single photon detection output charge distribution in 1 GHz BW with electronic noise 104 e
σ(Nout)
σnoise
Gain =1
ENF ~ 1
Gain ~ 100
ENF ~ 3…10
Gain ~ 1 M
ENF ~ 1.2
Gain ~ 1 M
ENF ~ 1.01
SiPM
N=0
N=2

## Slide 8: Methods
Measurements of
Charge response (typical in HEP)
DC current (typical in R&D of APD)

## Slide 9: ENF measurement method in HEP: charge response in photoelectrons on light pulse
Light (LED) and Dark (PED) measurements of charge histograms

## Slide 10: ENF measurement method in APD: dark and photocurrent mean and RMS
  Y-factor Method (switchable noise source)
  Cold Source & Network Analyzer
  Calibrated Noise Generator
  Power Spectral Density
  [1] Bertuccio, et al. (2024). Current Noise Spectral Density and Excess Noise of a Silicon Low-Gain Avalanche Diode (LGAD). IEEE Trans. Electron Devices, 71(10), 5845–5851.

## Slide 11: Results
Charge response measurements
by a short light pulse
Hamamatsu MPPC
Thorlabs FDS010
TAPD

## Slide 12: Photodiode mode (Gain = 1), oscilloscope LeCroy 6 GHz, Laser 535 nm, 40 ps, low intensity
Hamamatsu МРРС @10 V, Preamp 20 dB, 0.5 GHz BW
  Minimum signal ≈ 1 mV ≈ Electronic noise RMS
  Area (Charge) in a time gate 300 ns (white dotted line С2)
  Laser Charge (orange)

## Slide 13: Photodiode mode (Gain = 1), oscilloscope LeCroy 6 GHz, Laser 535 nm, 40 ps, medium intensity
Hamamatsu МРРС @10 V, Preamp 20 dB, 0.5 GHz BW
  Medium signal ≈ 8 mV >> Electronic noise RMS ≈ 1 mV

## Slide 14: Results in photodiode mode (Gain = 1)
Signal Sigma σ(Npe) ~ 10% Mean μ(Npe) – blue dots
  Pedestal σ(Electronic noise) ~ 105 е – black dots
  Poisson model – green line
Chart: Sigma(Npe) vs Mean(Npe)
| 17653416.149068322 | 14501242.236024845 | 2818633.5403726711 | 448633.54037267121 | 462484.47204968921 | 1468571.4285714289 | 3003291.9254658381 | 15526708.074534161 | 18286211.180124223 | 18054037.267080743
Sigma(Q) | 1947031.702 | 1424106.5943 | 284683.3344 | 46481.544 | 50578.5745 | 154775.4303 | 308294.1576 | 1546562.3623 | 1920589.8901 | 1888828.5757
SigmaPoiss | 4201.5969 | 3808.0497 | 1678.8787 | 669.8011 | 680.0621 | 1211.8463 | 1733.0008 | 3940.3944 | 4276.238 | 4249.0043 | 6796.784 | 1055.1559
DARK Sigma | 113043.4783 | 112857.1429 | 125652.1739 | 112919.2547 | 113664.5963 | 114223.6025 | 114534.1615 | 116335.4037 | 118198.7578 | 118571.4286 | 134596.2733 | 112919.2547

## Slide 15: Photodiode (Gain = 1) and Avalanche (Gain = 2.3) modes
Sigma(Npe) ~10% Mean(Npe) confirmed for Gain = 2.3
  MPPC is measured @ 50 V – two orange dots @ two Laser intensities
  No avalanche noise is observed
Chart: Sigma(Npe) vs Mean(Npe)
| 46196273.291925468 | 1113354.0372670807
Sigma(Q) | 4882617.2334 | 124492.1321
Sigma(Q) | 1947031.702 | 1424106.5943 | 284683.3344 | 46481.544 | 50578.5745 | 154775.4303 | 308294.1576 | 1546562.3623 | 1920589.8901 | 1888828.5757
SigmaPoiss | 4201.5969 | 3808.0497 | 1678.8787 | 669.8011 | 680.0621 | 1211.8463 | 1733.0008 | 3940.3944 | 4276.238 | 4249.0043 | 6796.784 | 1055.1559
DARK Sigma | 113043.4783 | 112857.1429 | 125652.1739 | 112919.2547 | 113664.5963 | 114223.6025 | 114534.1615 | 116335.4037 | 118198.7578 | 118571.4286 | 134596.2733 | 112919.2547

## Slide 16: Advices from Yu. Musienko (CMS CERN) based on experience in ENF APD 1990-2000е [3]
Electronic noise to be as low as 102 е
  Low noise FE electronics is a must
      Low BW
      Shaping
      Cooling
      Low noise power supply
Instability to be as low as 0.1%
    Laser instability as high as ~ 3%
    LED is typically preferable
    LED to be carefully selected
    LED driver to be carefully selected
    Thermal stabilization of preamp
[3] A. Karar, Y. Musienko, J. Vanel, Characterization of avalanche photodiodes for calorimetry, Nucl. Instr. Meth. Phys. Res. Sect. A, 428 (1999) 413–431.

## Slide 17: Analysis of the problems
Suppression of absolute noise of electronics
  => σ(Npe) = √μ(Npe) > σ(Electronic noise) ~ 105 е
  => μ(Npe) = σ(Npe)2 > 1010 е
Suppression of relative signal instability
  => σ(Npe)/μ(Npe) = 1/√μ(Npe) > (Non-Stab) ~ 0.1
  => μ(Npe) < 1/(Non-Stab)2 = 102 е
Trade-off for μ(Npe)
  σ(Electronic noise)2 < μ(Npe) < 1/(Non-Stab)2
  To be resolved only if σ(Electronic noise)  (Non-Stab) < 1
  E.g. Musienko’s example: σ(Electronic noise) = 100, (Non-Stab) = 10-3
The trade off is also resolvable at high avalanche gain

## Slide 18: Geiger mode (Gain ~ 1M), oscilloscope LeCroy 6 GHz, Laser 535 nm, 40 ps, a few photon intensity
МРРС (Hamamatsu) 1х1 mm2 @ 73 V (+1.5 V overvoltage)
  μ(Npe) ~ 1, ENF ~ 1.5 (optical crosstalk ~ 30%)
  σ(Npe)/μ(Npe) ~ 100% >> (Non-Stab) , σ(Npe) ~ 106 е >> σ(Noise)

## Slide 19: Possible solutions for low-gain ENF measurements
Tuning of the charge method toward lowest noise and instability
  New Preamp + cooling
  Selection of LED + driver in a pulse current stabilization mode
  Goal: μ(Npe) < 104 e, σ(Npe) < 102 e, (Npe) < 0.1%
To buy «noise figure meter / analyzer»
To develop «noise figure meter / analyzer»
To try DC current power spectral density method
  Avalanche current noise σ(I) in BW
  Avalanche current Power Spectral Density PSD(I)

## Slide 20: Thank you for your attention!
Sergey Vinogradov
vinоgradovsl@lebedev.ru

## Slide 22: Результаты измерений SiPM от лазера 40 пс 535 нм осциллограф LeCroy, фотодиодный режим
Измерения МРРС в фотодиодном режиме при 10 В (Gain = 1)
Максимальный сигнал около 50 мВ >> шума
  шкалы гистограмм отличаются в 5 раз

## Slide 23: Результаты измерений TAPD от белого LED 30 нс осциллограф R&S, фотодиодный режим
Измерения TAPD – почти нет зависимости σ(Qpe) от μ(Qpe)
  Разброс, нечеткие результаты (нестабильность TAPD?)
  Часто σ(Qdark) @LED=OFF > σ(Qphoto) @LED=ON

## Slide 24: Input-dependent characteristics of output (SNR, RES) Internal characteristics of photodetection (DQE, ENF)
Resolution → ENF
Signal-to-Noise Ratio → DQE
Signal (μN, σN)
Noise (μ = 0, σ = ENC)
Total Signal (μK, σK) + Noise(0, ENC)

## Slide 25: Resolution (RES) and Excess Noise Factor (ENF) of stochastic processes in photodetection
Resolution at output = Total ENF-times degraded Resolution at input
Total ENF is a product of Specific ENFs
Input photon distribution Photodetection processes Output charge distribution
RES(N)
RES(K)
ENFPDE
ENFGain

## Slide 26: ENF of simple specific processes
Multiplication (Xin=1)
Yout of any distribution
Photon count (Xin=1)
Bernoulli distribution
Dark counts (Xin=Npe)
Npe and Ndark ~ Poisson distribution
Xin=1
PDF(Yout)
PDF(Xin)=δ(x)
Yout=Gain
Photoelectrons
RES(Yout)
Dark counts
Xin=1
PDF(Yout) = Bernoulli
PDF(Xin)=δ(x)
Yout = PDE
Yout = Npe+Ndark

## Slide 27: Ideal detector
Ideal detector: conversion of any input light signal starting from single photon to recognizable output without noise and distortion in amplitude and timing of the signal
W. Farr, SPIE LEOS 2009
Ideal photon detector
Real photon detector

## Slide 28: SiPM calibration for CMS
Npe, Gain, ENF, Crosstalk = ECF:
  4 unknown @ 2 measured (Mean & Var)
  Unresolved SER and PE spectrum = unresolved unknowns
Assumptions / models to be applied to resolve the problem

## Slide 29: APD calibration for ENF
Npe, Gain, ENF, Crosstalk = ECF:
  3 unknown @ 2 measured (Mean & Var)
Xin=1
PDF(Yout)
PDF(Xin)=δ(x)

## Slide 30: Методика измерений ENF по току и заряду от световых импульсов с частотой F
Npe, Gain, ENF - 3 unknown
  1, 2 = Mean & Var – по гистограмме заряда на осциллографе
  3 = Npe = Ipe/F/q – по току Keithley при Gain = 1
  => ENF = Npe*Res2 (референс: ENF = 1 при Gain = 1)

## Slide 31: Шум осциллографа LeCroy @ 500МГц ~ 68 мкВ ~ 3 нВ/√Гц

## Slide 32: Шум предусилителя (4 ГГц 20 dB) ~ 248 мкВ ~ 11 нВ/√Гц

## Slide 33: Оценки возможности измерений по постоянному току
Сигма тока 1 мкА ~ 10 нВ @ BW = 100 KГц, R = 50 Ohm
  + предусилитель ~ 20 dB
  + селективный нановольтметр с частотным фильтром (Unipan)