## Slide 1: SPD Магнит Отчет – 3-й этап

## Slide 2: SPD Magnet (geometry)
Cryostat: Outer diameter -4008 mm;
Inner diameter - 3468 mm;
Length 4220 mm;
Thickness - 270 mm;
Cold mass: Outer diameter -3756 mm;
Inner diameter - 3662 mm;
Length 3416 mm;
Coils: (2 pieces): Number of layers - 2; Number of turns 2x156=312.
(1 piece): Number of layers - 2; Number of turns 2x78=156
Total number of turns - 780
Weight: - cryostat - 16700 kg
- shield - 1000 kg
- cold mass - 5390 kg
Total: ~23 t

## Slide 3
SPD Magnet
The main characteristics of the magnet:
Magnetic field along the axis - 1.0T with uniformity ± 2%;
The current is 5200 A.
Conductor type: Rutherford type cable consists of 8 strands with a diameter of 1.4 mm and a Cu / NbTi ratio of one, extruded into a matrix of high purity aluminum Al996, the conductor cross-section at a temperature of 4.5K is 7.90mm in width and 10.90mm in height;
Switching box
Cryostat
Coil
Shield

## Slide 4
Drawing of SPD Magnet

## Slide 5
Drawing of SPD Magnet

## Slide 6: Inner diameter is 4008 mm, Outer diameter is 3468 mm, length is 4220 mm. The thickness of the outer shell is 12 mm, the inner shell is 20 mm, the thickness of the flanges is 45 mm. The thickness at the ends of the shells is 40 mm. Material: St. Steel. The weight of Cryostat is ~16.7 t
Cryostat

## Slide 7
Drawing of Cryostat

## Slide 8: Material - aluminum alloy AMg-5. Outer diameter - 3898 mm, inner diameter - 3568 mm, length - 3720 mm. Wall thickness - 4 mm, Shield weight ~1 t
Thermal shield 80K
Gap
Insulator G10
For the collector, a 12x12 with 8 mm hole Al profile welded to the shell of the shields is used. The shield is divided around the perimeter into 4 parts using СТЭФ insulators. Outside the shield is covered with 30 layers of MLI and inside surface of the shield is covered with 10 layers of MLI .
The shield is positioned in the cryostat using ball bearings with an insulating ring (4 rows at the bottom and 2 rows at the top).
Collector

## Slide 9
Drawing of Shield

## Slide 10
Drawing of Shield

## Slide 11: Cold Mass (design)
2 coils x 2 layers - 312 turns
1 coil x 2 layers - 156 turns
10.95 мм x 7.93 мм,
NbTi / Cu d=1.4 мм
Magnetic field - 1 T
Current - 5.2 kA
36 x M12
64 x M12
Conductor mechanical and electrical parameters.
Rutherford cable, 8 strands, extruded in Al matrix
Thickness (after cold work) at 300 K | mm | 7.93 | ± 0.03
Width (after cold work) at 300 K | mm | 10.95 | ± 0.03
Critical current (at 4.2 K, 5 T) | A | > 14690 | 
Critical current (at 4.5 K, 3 T) | A | > 16750 | 
Overall Al/Cu/sc ratio |  | 10.5/1.0/1.0 | 
Aluminum RRR (at 4.2 K, 0 T) |  | > 600 | 
Al 0.2% yield strength at 300 K | MPa | > 30 | 
Rutherford cable is used to wind the coils. The cold mass consists of three coils, The coils are fixed together using bolts. If necessary, we will use special shims between the sections of the coils.

## Slide 12: The connection of the coils to the current leads is made through bas-bars with a cross section of 32 by 5.6 mm. The connection is made by welding. Thermal bridges made of high purity aluminum are used for temperature equalization.
Cold Mass
Bus-bars
Thermobriges
Manifold
Support brackets
coil-to-coil and layer-to-layer joints
Coil winding

## Slide 13: For front and back coils, cable length ~ 3600 meters; for the central coil the cable length is ~1800 meters. For cooling, a tube with a cross section of 14x14 mm and a hole of 10 mm is used, welded to the shell of the cold mass. Bimetallic adapters are used to connect aluminum profiles to stainless steel pipes.
Cold Mass
Out
In
Bimetal Al-St.Steel.
Collector

## Slide 14
Drawing of Cold mass

## Slide 15
Drawing of Cold mass

## Slide 16: Fixed support
SPD Magnet (Suspension system)
Sliding support
Fixation of the cold mass is made with help of triangular suspensions made of СТЭФ-1, 12 pieces on each side. On one side the supports are fixed, on the other side its are sliding to compensate for temperature changes in the length of the coil. The Suspensions have spherical bearings to avoid bending during thermal changes in the dimensions of the cold mass.
Spherical bearing

## Slide 17
Chart: Dependence of the deviation of the triangular suspension of the SPD cryostat on the load at a temperature of 300K/ 100K
| 200 | 400 | 500 | 700 | 800 | 1000 | 1200 | 1400 | 1500 | 1600 | 1700 | 1800 | 2000
T300_21_11 | 2 | 3 | 3.5 | 4 | 4.3 | 5 | 5.5 | 6 | 6.5 | 7 | 7.4 | 7.7 | 8.4
T100K_24_11 | 0.8 | 1.5 | 2.2 | 3.2 | 3.5 | 4 | 4.5 | 5 | 5.2 | 5.5 | 5.7 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5
Destruction of the suspension 300К - 3920 kg
Destruction of the suspension 100К - 4250 kg
We have made and tested the suspension at 300K and 100K
Drawing of suspension

## Slide 18: SPD Магнит with Control Dewar
Connection of current leads with Bas-bars coils.
The connection of the coil with the current leads is carried out in a special box located outside the cryostat.
Switching box
Current leads

## Slide 19
SPD solenoid. Cold mass cooling design.
It is planned to use the thermosiphon method of cooling the superconducting coil due to the natural convection of two-phase helium.
The volume of liquid helium is 10 - 20 liters
Helium mass flow SPD - 9-10 g/sec.

## Slide 20
Drawing of SPD Магнит with Control Dewar

## Slide 21
Drawing of Control Dewar

## Slide 22
To assemble the magnet, a special stand with an I-beam - 700 GOST 26020-83, 9 meters long, with a guide rail and a roller system (Roller skate Boerkey model AM-H) for rolling up the magnet elements, is used. Such a scenario was used to assemble the PANDA magnet, which was successfully assembled at the Votkinsk plant.
Magnet Assembly Procedure
Assembly stand
Roller skate Boerkey
Cryostat flange support
Cryostat Inner Shell Support
Inner Shield support
Cold mass support
Outer Shield support

## Slide 23
Magnet Assembly Procedure
Installing the outer shell
Installing the outer shield
Installing the Cold Mass
Position the outer shield
Position the Cold Mass. Fixing on temporary segments
Сегмент
Installing the inner shield

## Slide 24
Magnet Assembly Procedure
Installing the inner shell
Fixing of the cold mass on the inner shell. Removal of the temporary segments after fixing the cold mass. Installation all shield flange segments.
Shield flange segments
Installation of cryostat flanges
The Inner shield position. Partial installation of the shield flange segments
The Inner shell position.

## Slide 25
Calculation
Installation of cryostat flanges