## Slide 1
Swift heavy ions in radiation material science
V.A. Skuratov
Flerov Laboratory of Nuclear Reactions, Joint Institute for Nuclear Research, Dubna, Russia

## Slide 2
Swift heavy ions – ions with energies near and above 1 MeV/nucleon
E ≥ 1 МeV/nucleon
M ≥ 6 (Li)
Main sources of high energy ions:
Accelerators
Galactic cosmic rays
Fission fragments

## Slide 3
High energy heavy ion accelerator facilities:
GANIL (Caen, France) 1-100 MeV/amu
GSI (Darmstadt, Germany) 10-1000 MeV/amu
NSC (New Delhi, India) 15 MeV×Z
JINR (Dubna, Russia) 1.2-10 MeV/amu
CRC (Louvain-la-Neuve, Belgium) 0.6-27.5 MeV/amu
ANU (Canberra, Austarlia) 15.5 MeV×Z
RIKEN (Tokai, Japan) 7-135 MeV/amu
JAERI (Takasaki, Japan) 2.5-90 MeV/amu
ISRC (Astana, Kazakhstan) 0.42-1.67 MeV/amu
BNL (Berkeley, USA) 4.5-55 MeV/amu

## Slide 4
The composition of galactic cosmic rays includes:
83% protons
13% alpha particles
3% electrons
1% heavy ions (Z>4)
II. Galactic cosmic rays
Nuclear charge (Z)

## Slide 5
Electric field
e-
h+
SEE cross-section =
LET - Linear Energy Transfer [MeV×cm2/mg]
LET range: threshold LETtr ÷ ≈ 100 MeV×cm2/mg
SEE – Single Event Effects

## Slide 6
SEE – Single Event Effects
Todd Weatherford. FROM CARRIERS TO CONTACTS, A REVIEW OF SEE CHARGE COLLECTION PROCESSES IN DEVICES, 2002 IEEE NSREC Short Course

## Slide 7
WEIBULL FIT of threshold curve
s= σsat {1-exp[-(L-Lth)/W]S}
σsat : saturation value
Lth: threshold LET value
W and S are fitting parameters
Alessandro Paccagnella. Single Event Effects: Introduction
Scuola Nazionale di Legnaro. 29/3/2007

## Slide 8
IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. 50, NO. 3, 2003
Example cross-section curves for a Matra 32 K 8 SRAM

## Slide 9
FLNR accelerator complex.
Some crucial points for the SEE testing
Ion energy 3 - 50 MeV / nucleon
Beam intensity: 101 ÷ 105 сm-2s-1
Beam uniformity: ≤ 30 %
Energy accuracy: 10 %
Ion range in Si:  30 mkm (ion energy > 3 MeV/nucleon)
Dedicated beam operation time for testing: 2000 hours per year

## Slide 10
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics
…first step in 2007
The first dedicated beam line for low energy (3-6 MeV/nucleon)
Irradiation area: 80*160 mm.
Beam uniformity better than 30%
Beam intensity 10 ÷ 105 cм-2s-1 .
Low energy beam line on the base of U400

## Slide 11
U400M experimental hall.
High energy (14-40 AMeV) ion beam-line
Low energy (3-6AMeV) ion beam-line
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 12
Bending magnet
X-Y correction magnets
X-Y scanning system (50 Hz)
Ta foils (5-27 m) drive
Luminophore drive
Faraday cup
Turbo molecular pumps
Vacuum gate valve
Test chamber
Low energy ion beam line.
TOF measurement
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 13
Irradiation chamber for LE
Dedicated beam-line for high energy (3 ÷ 6 MeV/nucleon)
ions (usially Ne, Ar, Kr, Xe, Fe or Bi)
Irradiation area – 200x200 mm2.
Beam uniformity better then 30%
Beam flux 1 ÷ 105 cm-2s-1
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 14
Main components of the high energy beam-line.
vacuum gate valve (1 and 9)
quadrupole lenses
steering magnets
turbo molecular pumps
beam monitoring system (5, 6, 8, 10, and 11)
energy measurement system
the user target chamber
remote movement
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 15
Irradiation chamber for HE
Design of the experimental chamber allows:
the SEE testing in vacuum (10-2 torr) and air ambient
irradiation area of 60 mm in diameter.
automatic movement of the DUT in two orthogonal axes
(X and Y) in respecting of the beam direction (Z)
to change beam incident angle in the range of 0-90 degrees.
installation of degraders set.
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 16
DECRIS-SC2 superconducting
DECRIS-2 “warm”
From Li to Xe
From Kr to Bi
ECR source modernization up to the DECRIS-SC2 level
The main motivation of this update is the production of high charge state heavy ions which could boost the available beam energy and beam currents out of the U-400M cyclotron. On the other hand, another goal of the DECRIS-SC2 is to develop a compact superconducting ECR ion source with a high performance at 14 GHz which allows replace easily old room temperature ion sources from both cyclotrons keeping many existing subsystems.
the new ECR ion source is designed for high LET and high penetration of the DUT
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 17
The NEW low energy ion bean line on U400
Main features of the new facility are:
200 mm x 155 mm irradiation area
beam uniformity over irradiation area better then 10%
Ne, Ar, Fe, Kr, Xe, Bi ions with 3-6 MeV/nucleon
LET range of 4.5-100 MeV/(mg/cm2).
Fluent energy variation in the U400R will allows changing the ion energy without degraders.
Dubna, 23/01/2015
41st meeting of the PAC for Condensed Matter Physics

## Slide 18
Ion beam diagnostic
SEM micrograph of polymer track detector
Polymer track detector and the DUT
Etching threshold for ion tracks in
polycarbonate – 2.5 MeV/(mg/cm2) (O, Ne)
polyethylene terephthalate – 8 MeV/(mg/cm2) (Ar÷Bi)

## Slide 19
Ion beam diagnostic
SEM micrographs pictures of the track detectors surfaces irradiated under 30o tilted and normal 56 MeV oxygen ion beam incidence
9.55×106 cm-2
1.48×106 cm-2

## Slide 20
Ion beam distribution over the irradiating area
Ar, 120 MeV
Bi, 490 MeV

## Slide 21
ION BEAM PARAMETERS USED FOR SEE TESTING AT U-400M FLNR JINR CYCLOTRON
Ion type | Energy, MeV | LET, MeV/(mg/cm2) | Ion flux, cm-2s-1
16O | 56±3 | 4.5 | 1 ÷ 105
22Ne | 65±3 | 7 | 
40Ar | 122±7 | 16 | 
56Fe | 213±3 | 28 | 
84Kr | 240±10 | 41 | 
136Xe | 305±12 | 67 | 
209Bi | 490±10 (820±20) | 95 (100) | 

## Slide 22
III. Fission fragments

## Slide 23
Energy spectrum of U235 fission fragments
induced by thermal (a) and 2.5 MeV (b) neutrons.
Stephen S. Friedland. Phys. Rev. 84(1951), 75
Mass distribution of fission fragments from Pu239.
Solid line is coincident fragment experiment; dashed line is chemical analysis.
D.C.Brunton and W.B.Thomson. Phys. Rev. 76(1949), 848
a
b

## Slide 24
D. Staicu. Radiation damage modeling
in oxide, nitride and carbide fuels

## Slide 25
Scheme of ion track formation process
Main peculiarity of swift heavy ion interaction with solids is a high level of ionizing energy losses which may result in formation of specific radiation damage – latent tracks
Nanostructuring may enhance localization of energy deposition in the ion trajectory region and affect the latent track formation processes
 1%  99%
(-dE/dx)t = (-dE/dx)n + (-dE/dx)ion

## Slide 26
TEM image of tracks from 235U fission fragments in a synthetic fluor-phlogopite mica.
R.L., P.B. Price, R.M. Walker: "Nuclear Tracks in Solids: Principles and Applications." University of California, Berkeley, 1-605, (1975)

## Slide 27
Accelerator for applied research – IC100
B+2, Ne+4, Ar+7, Kr+17, Xe+26 ions with energy  1.2 MeV/amu
Ion fluence range – up to 1015cm-2

## Slide 28
DC-60 CYCLOTRON (Astana)
E= 0.42-1.75 MeV/amu

## Slide 29
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
High energy heavy ion irradiation testing of materials that show promise for nuclear applications:
inert matrix fuel hosts: oxides (Al2O3, MgO), spinels, carbide and nitride based ceramics (ZrN, Si3N4, AlN)
ZrN, TiNZrN coating layers on Zircaloy alloys
Oxide dispersion strengthened (ODS) steels
Our central objectives are:
to study the structural changes and mechanical stresses induced by swift heavy ions as function of ion fluence and ionizing energy loss
to elucidate the dense ionization effect on pre-existing defect structures in irradiated materials
to compare the radiation stability of nanocrystalline and bulk ceramics.
Inert matrices - ceramics with a high melting point and with low neutron absorption cross sections to be used as hosts for transmutation of actinides via nuclear reactions
Examples of fuel compositions for LWR:
(Pu)O2 - MgO-ZrO2
(Pu,Np,Am)O2, MgO-ZrO2
(Am,Np,Pu,Zr)N

## Slide 32
8,2 мм
M. Streit et al. Journal of Nuclear Materials 319 (2003), pp. 51–58

## Slide 34
VVER-1200 fuel assembly

## Slide 35
VVER-1000 fuel pin design

## Slide 36
C. Kinoshita. Microstructural evolution of irradiated ceramics. In: Radiation effects in solids. Eds. K.Sickafus, E.Kotomin and B.Uberaga. Nato Science series. V.232, p.193
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
spinel is not amorphized by electron, neutron and low-energy ion irradiation at T > 300 K

## Slide 37
Ion tracks in spinel irradiated with 430 MeV Kr ions to a fluence of 1.11012 cm-2 at room temperature.
The average TEM track diameter is ~2 nm.
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
MgAl2O4
S.J. Zinkle, V.A. Skuratov . NIMB. B 141 (1998) 737

## Slide 38
Ion tracks in spinel irradiated with 430 MeV Kr ions
S.J. Zinkle, V.A. Skuratov . NIMB. B 141 (1998) 737
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
Swift heavy ions induce discontinuous nonamorphous tracks in spinel

## Slide 39
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
Cross-section microstructure of MgAl2O4 irradiated to a fluence of 1x1016 72 MeV Iodine ions/cm2
volumetric swelling is 35% for the crystalline to amorphous phase transformation
Calculated damage energy and electronic stopping power for 72 MeV I ions in MgAl2O4
S.J. Zinkle, Hj. Matzke, V.A. Skuratov, Mat. Res. Soc. Symp. Proc. 540 (1999) 299.

## Slide 40
Step heights formed on the surfaces of MgAl2O4 and Al2O3 along a border of masked and 85 MeV I+7 ion irradiated area. Ion fluence 1.2× 1015 cm-2
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
The swelling due to amorphization is estimated to be around 15–20%
T. Aruga et al. / NIM B 197 (2002) 94–100

## Slide 41
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
No amorphization occurs for MgO samples at the fluence of 1.2× 1015 cm-2
XTEM image of polycrystalline MgO sample irradiated with 85 MeV I+7 ions to 0.28× 1015 cm-2 (a) and 1.2× 1015 cm-2 (b)
T. Aruga et al. / NIM B 197 (2002) 94–100

## Slide 42
3D AFM image of of MgAl2O4 surface irradiated with 710 MeV Bi ions.
Ion fluence 5x1010 cm-2.

## Slide 43
128 MeV
25.4 keV/nm
495 MeV
39 keV/nm
710 MeV
41 keV/nm
E= 0 MeV
3D AFM images of -A2O3 surface irradiated with 5x1010 cm-2 Bi ions of different energies

## Slide 44
Examination of the dense ionization effect in ceramics and oxides with heavy ions of fission fragments energy
Material | Set, keV/nm | Ref.
AlN | > 34 | S.J.Zinkle, V.A.Skuratov and D.T.Hoelzer. NIMB 191(2002) 758
 | > 21.6 | S. Mansouri et al. // NIMB 266(2008) 2814
BN | > 17.6 | S. Mansouri et al. // NIMB 266(2008) 2814
SiC | >34 | S.J. Zinkle, J.W. Jones, V.A. Skuratov. MRS Symposium Proceedings, Vol. 650, MR, Warrendale, PA, 2001, p. R3.19.1.
SiC Nano-SiC | > 22 > 17 | A. Audren et al. // NIMB 267(2009) 976, NIMB 266 (2008) 2806
Nano-ZrN | > 49 | A. Janse van Vuuren, V. A. Skuratov, V.V. Uglov J. Nucl. Mater. 442 (2013) 507.
Si3N4 | 15 | S.J.Zinkle, V.A.Skuratov and D.T.Hoelzer. NIMB 191(2002) 758
Ionizing energy loss threshold values for latent track formation in nitrides and carbides

## Slide 45
5 m
10 m
1 m
100 nm
ZrN coating
5 m
3 m
V.V. Uglov et. al. // Surf.Coat.Technol., 204( 2010), 2095
Equipment for deposition
(VU-2MBS)
Formation of nitride coatings
    ZrN coatings were formed by Cathodic Arc Vapor Deposition (CAVD) technique.
    Pretreatment: p = 10–3 Pa, Ubias= -1 kV, IZr= 100 A.
    Deposition parameters: pN= 10–1 Pa, Ubias= – 120 V, IZr= 100 A.
    deposition time 15-18 s, 10-11 min, 40 min.
    Objects: CAVD coatings ZrN // Si

## Slide 46
TEM image of as-grown 80 nm ZrN layer
Bright field TEM micrograph of virgin ZrN sample
Radiation stability of nanocrystalline ZrN against swift heavy ion irradiation

## Slide 47
2.5x1013
5x1012
1x1013
5x1014
3x1012
1x1014
FFTs of the ZrN after irradiation with Xe ions to fluences from 3x1012 to 5x1014 ions/cm2
TEM (100 nm / 167 MeV Xe)

## Slide 48
Centre for High Resolution Transmission Electron Microscopy
TEM (10 μm / 695 MeV Bi, 250 MeV Kr)
Selected Area Diffraction of the 10μm ZrN layers before irradiation and after irradiation with Kr ions (top row) and Bi ions (bottom row) at doses ranging from 1x1012 to 7.06x1013 ions/cm2
1x1013 Kr
3x1013 Kr
7.06x1013 Kr
As Deposited
1x1012 Bi
1x1013 Bi
3x1012 Bi
7x1012 Bi
Ring Pattern Simulation for ZrN

## Slide 49
Results (XRD)
X-ray diffraction patterns recorded on virgin and swift heavy ion irradiated nanocrystalline ZrN samples
Xe, 167 MeV
Bi, 695 MeV
The phase composition of nanocrystalline ZrN is not changed after heavy ion irradiation at electronic stopping power up to 49 keV/nm
TEM examination does not reveal latent tracks formation in ZrN irradiated with heavy ions of fission fragments energy

## Slide 50
ODS = Oxide dispersion strengthened alloys:
Thermally stable oxide nanoparticles dispersed in ferritic matrix
Strengthening principle in ODS alloys:
NPs are obstacles to dislocation glide
Production:
mechanical alloying of metal-oxide powders / sealing / extrusion or hot pressing
High performance at elevated temperatures:
High creep strength
High radiation resistance
Low swelling under neutron irradiation
Radiation stability of ODS alloys against fission fragment impact
Y4Al2O9 nanoparticles in KP4 ODS steel

## Slide 51
Motivation
Radiation stability of oxide nanoparticles in ODS alloys against swift heavy ion irradiation simulating fission fragments impact
Scanty information about dielectric nanoparticles in metal matrices irradiated in electron stopping regime

## Slide 52: Cr16 ODS alloy (Y2Ti2O7, Y2TiO5, Cr23C6)
Ferritic grain with large Y-Ti oxide particles (A), dislocations and Cr23C6 grain (B)
SAD patterns: orthorhombic (o) and fcc (с) Y-Ti oxides
Cr23C6 grain
Y-Ti-O

## Slide 53: Cr16 ODS alloy
BF image and SAD pattern of α-Fe matrix with Me23C6 particle
(Cr,W)23C6

## Slide 54: EP450 ODS alloy
Coherent Y2Ti2O7 (cubic) oxides in α-Fe matrix
Oxide size distribution →
d = 5 - 200 nm; ‹d› = 10 nm; concentration ~ 1015 cm-3

## Slide 55
Se = 53 keV/nm
Cr16/ Bi 700 MeV/ 1.5×1012cm-2
Amorphous tracks in Cr23C6 carbide grain
(cross-sectional BF, SAD)

## Slide 56
EP450/ Xe 167 MeV/ 1×1012cm-2
Se = 35 keV/nm

## Slide 57
The upper limit of Se threshold value in Me23C6 carbides is estimated to be around 35 keV/nm
EP450/ Xe 167 MeV/ 1×1012cm-2
Se = 35 keV/nm
No latent tracks of high energy heavy ions are registered in carbides

## Slide 58
Amorphization of Y-Ti oxides induced by irradiation in the ion track overlapping regime (plane view DF, SAD)
Cr16/ Bi 700 MeV/ 1.5×1013cm-2

## Slide 59
Cr16/ Bi 700 MeV/ 1.5×1013cm-2

## Slide 60
EP450/ Xe 167 MeV/ 1×1012cm-2

## Slide 61
HRTEM and DF TEM micrographs of latent tracks in Y2Ti2O7
EP450/ Xe 167 MeV/ 1×1012cm-2
Se = 23 keV/nm

## Slide 62: EP450/ 26 MeV Xe/1012 cm-2
Amorphous tracks in Y2Ti2O7 particle (plane view DF, HR, SAD)
Se =9.5 keV/nm

## Slide 63
Mean track diameter is 7.5 nm
15CRA-3/ Xe 167 MeV/ 1×1012cm-2
Se = 23 keV/nm

## Slide 64
Latent track diameter as a function of stopping power for various ions in Y2Ti2O7

## Slide 65
Main questions addressed to real-time measurements:
Radiation damage and stress accumulation processes before and
after ion track region overlapping
Variation in the stress state under ion irradiation characterized
by specific ionizing energy losses higher and lower than the threshold
of radiation damage formation via electronic excitations.
Accumulation of mechanical stresses under swift heavy ion irradiation
The knowledge about of high energy heavy ion-induced stress is of considerable practical value in view of simulation of fission product impact in radiation resistant oxides and ceramics, considered as candidate materials for nuclear waste management (inert matrix fuel host)

## Slide 66
Basis of the piezospectroscopic effect – the applied stress strains the lattice and alters the energy of transitions between electronic states
 = ij×ij
ij – piezospectroscopic coefficients
Typical piezospectroscopic probes: Cr3+ in Al2O3
Eu3+, Nd3+ in silica glasses
Sm3+ in borosilicate glasses
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION
R1-line
R2-line
D. Clarke et. al.

## Slide 67
Dose dependence of ionoluminescence spectra in Al2O3 and MgO measured during
167 MeV Xe ion irradiation at 80 K.
Al2O3 MgO

## Slide 68
Ion fluence, cm-2
wavenumber, cm-1
Kr
Xe
Bi
ii, iii
Se=41 keV/nm
Se=25 keV/nm
Se=16 keV/nm
The stresses are compressive in basal plane of the sample and tensile in perpendicular direction
each Cr3+ ion acts as an independent strain sensor
The splitting of the R-lines directly indicates on the presence of differently stressed regions in the irradiating ruby specimen

## Slide 69
wavenumber, cm-1
Ion fluence, cm-2
Xe
Se=25 keV/nm

## Slide 70
167 MeV xenon ion induced tracks in Al2O3.
Ion fluence is 2×1013 cm-2.

## Slide 71
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION
1=3.26(11+22)+1.5333
2=2.73(11+22)+2.1633
ii (i = 1, 2, 3) – stress tensor components, oriented along a, m and с axes
Bi,700 MeV
Xe,167 MeV
Kr,107 MeV

## Slide 72
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION

## Slide 73: 167 MeV Xe in Al2O3

## Slide 74
J.H. O’Connell et al., NIM B (2015), http://dx.doi.org/10.1016/j.nimb.2015.09.067
Normalized density variation as a function of radial distance from the track center (MD simulation)
Two experimental plots of 1 mean basal plane lattice dilation as a function of radial distance from the track center (TEM images processing)

## Slide 75
Thank you for your attention!