## Slide 1: Current-Voltage Characteristics of Aluminium and Zinc Implanted Silicon for Radiation Detection Applications Duke Ateyh Oeba
Department of Physics
University of South Africa

## Slide 2
Introduction
    Semiconductor detectors
    Silicon detectors
    Dopant
    Application of detectors
Problem statement
Literature review
Experimental procedure
Results and discussion
conclusion
Acknowledgement
OUTLINE

## Slide 3: Semiconductor detector
Semiconductor detectors are instruments designed for detection and measurements of charged particles and rays
The interaction of radiation with semiconductor material generates, electrons and holes, carriers
Electrons and holes are collected to the electrodes where they result into electrical signal [1]
INTRUDUCTION
[1] Aurola, A., 2018. Semiconductor radiation detector. U.S. Patent Application 10/079,325.

## Slide 4: Why Silicon detectors
  Low leakage current [1]
  Superior energy resolution [2]
  High radiation sensitivity [3]
  Work well at room temperature [3]
  High signal to noise ratio
[1] Bortoletto, D. (2015). How and why silicon sensors are becoming more and more intelligent?
[2] Khelil et al. (2018). The effects of doping type on structural and electrical properties of silicon nanocrystals layers grown by plasma enhanced chemical vapor deposition
[3] Mirzaei et al. (2018). Room Temperature Hard Radiation Detectors Based on Solid State Compound Semiconductors:
Notes: Due to relatively wide band gap of Si (1.12eV), silicon diode detectors can be operated at room temp.

## Slide 5: Dopant -Al and Zn
Abundant
Cheap
Low electrical resistivity Al (3μΩ-cm)[1]
Fastest diffusion dopant [1]
[1] Kumar et al. (2018). Comparison of Silicon, Germanium, Gallium Nitride, and Diamond for using as a detector material in experimental high energy physics

## Slide 6
Application of Detectors
In High Energy Physics Experiments
In industrial imaging and material processing
For medical imaging
In biomedical diagnostic
Notes: HEP experiments to detect charged particles

## Slide 7
Problem Statement
    Radiation detectors get damaged-
        High leakage current [1]
Small detector volume
Radiation induced defects
    Increase in free carrier trappings
High energy to separate charge carrier
[1] Moscatelli et al. (2016). Combined bulk and surface radiation damage effects at very high fluences in silicon detectors:

## Slide 8
Literature review
Megherbi, M. Larbi, et al. "Analysis of Trapping Effects on the Forward Current–Voltage Characteristics of Al-Implanted 4H-SiC pin Diodes." IEEE Transactions on Electron Devices 65.8 (2018): 3371-3378.
    High recombination rate, decrease carrier mobility, high resistance
    Effect on forward current
    small detector volume
Moloi, S. J., & McPherson, M. (2009). Current–voltage behaviour of Schottky diodes fabricated on p-type silicon for radiation hard detectors. Physica B: Condensed Matter, 404(16), 2251-2258.
  Erbium, Niobium, Gold
  Defect levels generated by metal in silicon
  Expensive metals

## Slide 9
EXPERIMENTAL PROCEDURE
Implantation energy 160K, fluence 1017 ions cm-2
Cleaning was done using standard procedure[1]
Schottky contacts-gold, Ohmic contacts-Al [1]
Deposition pressure 10-6 mbar, rate 1Å/s
I-V measurements taken at room temperature
Data range -2V to 2V, voltage step 0.01V
[1] Derry, T. E., Lisema, L. I., Magabe, A. T., Aradi, E., Machaka, R., & Madhuku, M. (2018). Allotrope conversion and surface hardness increase in ion implanted boron nitride. Surface and Coatings Technology, 355, 61-64.

## Slide 10
RESULTS AND DISCUSSION
Figure 1(a) and (b): Current-voltage characteristics of detector fabricated on Undoped, Al, and Zn-doped p-silicon in a linear scale
Reverse current is higher in Al-doped than undoped diodes
Forward current in all cases is linear at higher voltage (1V ≥)
Both figures exhibit diode behavior

## Slide 11
RESULTS AND DISCUSSION Cont..
Figure 2(a) and(b): Current-voltage characteristics of detector fabricated on Undoped, Al, and Zn-doped p-silicon in a linear scale
Forward current is Zn-doped higher than undoped diodes
Zn-doped exhibit ohmic behavior at lower voltage

## Slide 12
RESULTS AND DISCUSSION Cont..
Forward current is less in Zn than Al-doped
Zn-doped exhibit ohmic behavior
Figure 3(a) and(b): Current-voltage characteristics of detector fabricated on Undoped, Al, and Zn-doped p-silicon in a linear scale

## Slide 13
In Zn-p-Si, reverse bias current is almost equal to forward bias current
High forward bias current in Al-p-Si than Zn-p-Si
Current linear at lower voltage (-0.5V to 0.5V)
RESULTS AND DISCUSSION Cont..
Figure 4(a), (b) and(c) : Current-voltage characteristics of detector fabricated on undoped, Al, and Zn-doped p-silicon in a semi logarithmic scale
b
c

## Slide 14
Table: 1 A summary of device parameters evaluated from I-V plots fabricated on p-Si detector
Parameter | Undoped | Aluminum- doped | Zinc-doped
IS (μA) | 2.565 | 1.452 | 2.718
Ideality factor, η | 1.539 | 1.245 | 2.650
Schottky barrier height, Φ | 0.1814 | 0.1962 | 0.1892
η (2.65) in Zn-doped corresponds to high saturation current, IS
Low η (1.25) in Al-doped corresponds to high Φ
η is attributed to the impurity of the material and interface layer
Low IS (1.45μA) on Al-doped to undoped (2.57μA) is due to defects
RESULTS AND DISCUSSION Cont..

## Slide 15
The detector exhibited high resistivity.
The measured current is ohmic.
The ohmic behavior and the increase in resistivity is responsible for relaxation behaviour of the material
The relaxation material is resistant to radiation damage.
  Independent of incident radiation-radiation hard
CONCLUSION

## Slide 16: ACKNOWLEDGMENTS
Prof. S J Moloi
UNISA - Physics Department
NRF
iThemba LABS

## Slide 17
Questions and Comments
Notes: D A OEBA