## Slide 1: Prompt-gamma neutron activation analysis in mining.
Frank Laboratory of Neutron Physics Joint Institute for Nuclear Research
Author: Constantin Hramco, engeneer.
costea.edinets@mail.ru

## Slide 2: Presentation plan:
1. Introduction
2. Experimental work
3. Results and discussion
4. Conclusions

## Slide 3
1. Introduction
Medicine
Mining
Construction
Jewelry
Agriculture
Synthesis

## Slide 4
Our dashingly developing society needs more and bigger quantities of different materials for self-evolving. This type of requirements displays a lot of sectors of human activities, starting with food processing and ending with our brain evolution. Among these branches is placed the mining industry.
The neutron physics has large achievements in the elemental content determination area. An excellent example is the neutron activation analysis. The activation with thermal neutrons is too slow method for mining. That is why the solution is to use fast neutrons for prompt gamma neutron activation analysis (PGNAA).

## Slide 5
2. Experimental work
Three types of ore samples for analysis:
Concentrate – sample with highest concentration of P2O5 – 38.95%
Tail – sample with lowest concentration of P2O5 – 0.9%
Mixture – sample with concentration of P2O5 being between the values for first and second samples.
Controlled element | Apatite concentrate, mass % | Tails, mass %
P2O5 | 38.98 | 0.90
Al2O3 | 0.99 | 20.88
CaO | 50.58 | 4.90
SiO2 | 2.38 | 42.16
Fe2O3 | 0.68 | 8.02
K2O | 0.24 | 6.02
H2O | 0.06 | 0.15
TiO2 | 0.33 | 2.92
Na2O | 0.50 | 10.26
Table 1. Content of different controlled elements in phosphate ore.

## Slide 6
The sample is PET sac containing 10 kg of phosphate ore.
Phosphorite – Ca5(PO4)3+
ω(Ca) = 41.29%
ω(CaO) = 57.77%
ω(P) = 19.15%
ω(P2O5) = 43.87%

## Slide 7
For experimental setup source of neutrons was chose 239Pu-Be mixture with average neutron energy around 4.5 MeV. To detect gamma rays that are coming from interaction of neutrons with nuclei was set a Ortec high-purity germanium detector (HPGe) with the features presented in the table below:
 | Certified | Measured
Resolution (FWHM) at 1.33 MeV, 60Co | 1.90 keV | 1.90 keV
Relative Efficiency at 1.33 MeV, 60Co | 30% | 36%
Table 2. Main characteristics of Ortec HPGe gamma-detector.

## Slide 8
Used reaction
Inelastic scattering (n, n’ γ)

## Slide 9
In order to perform the objective, first step is to evaluate the accuracy of HPGe in detecting of gamma-radiation from different elements. This task was reached by assembling the construction that is shown in Figures below:
Figure 1. The scheme of assembly for determining
the elemental content of phosphate ores.
Figure 2. 3D-model of assembly for determining the elemental content of phosphate ores.
http://www.autodesk.com/solutions/3d-design-software

## Slide 10
Figure 3. HPGe Channel-Energy calibration curve.
Important step in work with any gamma-spectroscopy instrument is to have well done channel-energy calibration. In our case the calibration was performed by two methods: by standard point sources (60Co & 137Cs) and by irradiation of metal samples (Cd & Pb).
60Co : 1173.2 and 1332.5 KeV
137Cs : 661.7 KeV

## Slide 11
3. Results and discussions
The data acquisition was done by COCOS (COmbined COrrelation System) program developed at JINR FLNP, data processing was performed by Canberra’s Genie™ 2000 program. As an example, in the figure below is shown the comparison between gamma-spectra from three irradiated samples (concentrate – black, tails – red, mixture – purple) and background (blue):
Figure 4. Part of gamma-ray energy spectrum (2.0-2.5 MeV).
http://www.canberra.com/products/radiochemistry_lab/genie-2000-software.asp
http://www.originlab.com/

## Slide 14
In Figure 5 is shown the comparison between the measurements made with different types of detectors: HPGe (with high resolution) and BGO (with high efficiency). Although BGO has a higher efficiency of gamma-ray detection, it has a moderate energy resolution. For example: if we compare Figure 4 with Figure 5, especially the interval between 2.20 and 2.25 MeV, in case of HPGe we can see that there are three lines from different sources (27Al, background and 31P).
In case of BGO (Figure 5, green and dark-blue lines) these gamma-lines, either from concentrate or from tails samples, can not be divided.
Figure 4. Part of gamma-ray energy spectrum (2.0-2.5 MeV).
Figure 5. Comparison of the energy resolutions of HPGe and BGO detectors.

## Slide 15
γ-line energy, keV | Attachment (Concentrate/Tails) | Isotope | Table energy, keV
751 | Concentrate | SE 31P | 1266,13
766 | Concentrate | 44Ca | 761,12
843 | Mixture | 27Al 56Fe | 843,76 846,76
983 | Tails | 48Ti | 983,54
1014 | Tails | 27Al | 1014,52
1156 | Concentrate | 44Ca | 1157,02
1238 | Mixture, Tails | 56Fe | 1238,27
1266 | Concentrate | 31P | 1266,13
1369 | Mixture | 56Fe 39K | 1360,21 1360,60
1635 | Tails | 23Na | 1635,96
1811 | Mixture, Tails | 56Fe | 1810,76
2151 | Concentrate | 31P | 2148,40
2213 | Tails | 27Al | 2212,01
2237 | Concentrate | 31P | 2233,60 2239,80
2275 | Mixture, Tails | 56Fe 23Na | 2273,20 2276,13 2263,39
2523 | Mixture | 56Fe 39K | 2523,06 2522,40
2814-2846 | Tails | 28Si 27Al 48Ti 39K | 2838,29 2836,40 2819,08 2814,24
3132 | Concentrate | 31P | 3134,30
3223 | Concentrate | SE 40Ca | 3736,30
3732 | Concentrate | 40Ca 48Ti | 3736,30 3738,35
7580 | Mixture, Tails | 48Ti | 7585,00
In table 3 (on the right) is presented a part of detected elements. Although the work was done using different software there is no big shifting between acquired and table data. Nevertheless our assembly allowed to detect all elements presented in Table 1.
Table 3. Some of the identified gamma-lines in the acquired spectra.
www.nndc.bnl.gov
www.ndc.jaea.go.jp/jendl/j40/j40.html

## Slide 16
4. Conclusions
An experimental setup for determining the elemental composition of materials by prompt gamma-ray neutron activation analysis (PGNAA) was commissioned and tested.
The better accuracy of HPGe in detecting of elemental composition was confirmed.
The acquired spectra was processed and decoded successful.
Some preliminary results are reported and further actions proposed.

## Slide 17
Acknowledgement
D. N. Grozdanov
Yu. N. Kopach
V. M. Bystritsky
S. B. Borzakov
F. A. Aliyev
N. A. Gundorin
I. N. Ruskov
V. R. Skoy