## Slide 1: Positron studies of defects in ion-implanted materials
Dr. Krzysztof Siemek
Institute of Nuclear Physics PAN, Cracow, Poland
Joint Institute for Nuclear Research, Dubna, Russia

## Slide 2: Outline
Introduction - ion implantation
Positron Annihilation Spectroscopy
Results
Summary

## Slide 3: Ion implantation
Ion implantation is process by which ions of one element are accelerated into a solid target, thereby changing the properties of the target.
Adventages:
Low temperature processing
Good control and reproducibility of impurity implanatation depth
Solubility limits can be exceeded without precipitations of excess atoms
Applications:
Modyfing surfaces to improve properties
Fabrication of semiconductor devices
H. Abe, et. Al.. Trans. Mat. Res. Soc. Japan 36 (2011) 133

## Slide 4
Irradiation induces a large number of structural defects, such as vacancies, their clusters, dislocation loops, voids etc. As a result, swelling, hardening, creep and embrittlement appear and leads to a faster wear.
Amaya, M. et al., J. Nucl. Sci. Technol. 45(3) (2008) 244
Disadventages:

## Slide 5: Monte Carlo simulations using SRIM/TRIM*
TRIM calculations for silcion implanted with 25 keV Nitrogen
*software available on www.srim.org

## Slide 6: Energy deposition
a)
b)
*https://www-nds.iaea.org/stopping/

## Slide 7: Energy deposition
a) TRIM calculations for silcion implanted with 25 keV Nitrogen
b) TRIM calculations for silcion implanted with 5 MeV Nitrogen
Nuclear collisions

## Slide 8: Schematic representation of the disorder produced by ion implanation
Track region
Cascade region
Not implanted region

## Slide 9: Ion ranges and vacacncies distribution

## Slide 10: Long Range Effect
* Yu.P. Sharkeev, E.V. Kozlov, Surf. Coat. Technol. 158-159 (2002) 219
Dislocation structures formed in Cu implanted with the Ni ions.
Implantation range was about 20 um.
10 um
50 um
unirradiated

## Slide 11: Positron annihilation spectroscopy
PAS techniques allow us to find defects with the size ranging from 0.1 to 3 nm with the concentration up to 107 ppm
PAS makes possible the detection of defects in the wide range of depths from single nanometers up to milimeters
*) https://www.hzdr.de/db/Cms?pNid=3581

## Slide 12: Positron annihilation spectroscopy
PAS techniques:
angular correlations of gamma quanta
Doppler spectroscopy (DB)
positron lifetime spectroscopy (LT)
Possibilities:
determination of defect concentration
evaluation of defect concentration profile
detection of the kind/size of defects
* http://www.ifj.edu.pl/~mdryzek/
Applications:
solid body physics
material and surface engineering
metals, semiconductors, thin layers

## Slide 13: Positron Annihilation Spectroscopy
The annihilation rate λ - the reciprocal value of mean positron lifetime
r0 – electron radius, c – velocity of light
electron density inside the defect is lower in comparison to bulk area what finds a reflect in the mean positron lifetime
e.g. for pure Fe τ = 110 ps in nondefected structure while positron trapped inside vacancy lives τ = 174 ps
Bi

## Slide 14: Positron 22Na source
positron source: 22Na with activity of 1 MBq enclosed into a 10 mm Ti foil

## Slide 15
Disadvantages of experiment are a long range of positron implantation and a lack of possibility to locate positrons precisely on the given depth.
The conventional pas experiment
P. Horodek, J. Dryzek, Nukleonika 55 (2010) 17

## Slide 16: Positron annihilation spectroscopy
digital spectrometer: BaF2- based detectors and APU8702 unit
spectra including 106 counts were deconvoluted by LT code [*], substracting the background and the source components
*) J. Kansy, Nucl. Instrum. Method. Phys. Res. A 374 (2) (1996) 235

## Slide 17
The positron lifetime spectroscopy
positron lifetime spectra consists of the exponential decay components
positron trapping in the open-volume defects leads to long lived components
longer life time due to lower electron density
analysis by non-linear fitting: lifetimes ti and intensities Ii
Experimental techniques: LT spectroscopy
The example of positron lifetime spectrum.
The positron lifetime spectrum
The mean positron lifetime

## Slide 18
There are some areas i.e. thin layers, ion implantation, semiconductors where the application of conventional PAS experiments is strongly limited
HERE EXPERIMENTS WITH SLOW POSITRONS ARE REQUIRED !!
https://www.hzdr.de/db/Cms?pNid=3581
The conventional pas experiment

## Slide 19
The Variable energy positron beam

## Slide 20
from iThemba LABS (RSA)
The Variable energy positron beam

## Slide 21
The Variable energy positron beam

## Slide 22
The Variable energy positron beam

## Slide 23
The Variable energy positron beam

## Slide 24
Feature | Value
activity of 22Na isotope | ~30 mCi
moderator | frozen Ne (7K)
magnetic field | 100 Gs
vacuum conditions | 10-9 Torr
intensity | ~106 e+/s
energy range | 50 eV ÷ 40 keV
diameter of the flux | 5 mm
The Variable energy positron beam

## Slide 25: Positron Annihilation Spectroscopy
The change of photon energy by relativistic Doppler effect in the laboratory system
where EB is binding energy e+e- in the pair surrounding, p|| – momentum of annihilating pair, m – electron mass, c – speed of light in the vacuum.
S parameter
ratio of area under the central part of 511 keV line to whole area below this line
defines the participation of e+e- pairs with low momentum
higher value means bigger concentration of such defects as vacancies

## Slide 26: Positron Annihilation Spectroscopy
The change of photon energy by relativistic Doppler effect in the laboratory system
S parameter
ratio of area under the central part of 511 keV line to whole area below this line
defines the participation of e+e- pairs with low momentum
higher value means bigger concentration of such defects as vacancies

## Slide 27: Positron Annihilation Spectroscopy
The change of photon energy by relativistic Doppler effect in the laboratory system
W parameter
ratio of area under the wing part of 511 keV line to whole area below this line
defines the participation of e+e- pairs with high momentum
together with S parameter gives limited information about kind of defects

## Slide 28: ABINIT calculations
ABINIT is a package whose main program allows one to find the total energy, charge density and electronic structure of systems made of electrons and nuclei (molecules and periodic solids) within Density Functional Theory (DFT), using pseudopotentials (or PAW atomic data) and a planewave basis.
We have to know:
Pseudopotenitials
Information about stucture
Proper aproximation and settings
*https://www.abinit.org/about

## Slide 29: Results

## Slide 30: IRRADIATION
The irradiation was performed at IC-100 cyclotron at Flerov Laboratory of Nuclear Reactions at JINR in Dubna. Xe26+ heavy ions with energy 167 MeV and different doses were applied. The average ion flux was 5×109 cm−2 s-1. Temperature did not exceed 80 ˚C.

## Slide 31: Results: Pd
*) P. Horodek, V.A. Skuratov, Surf. Coat. Technol. 296 (2016) 66.

## Slide 32: Results: Pd
The mean implantation depth for given energy E is estimated from
where A=3.67 mgcm-2keV-n, n=1.579 and r is density equal 12.023 g/cm3.
Diffusion equation
*) P. Horodek, V.A. Skuratov, Surf. Coat. Technol. 296 (2016) 66.

## Slide 33: Results: Pd
Defect concentration
where:
- trapping coefficient (for given type of defect)
tbulk - positron lifetime in bulk
Lbulk - positron diffusion length
*) P. Horodek, V.A. Skuratov, Surf. Coat. Technol. 296 (2016) 66.

## Slide 34: Etching experiment

## Slide 35: Results: Fe
*) P. Horodek, et al., Rad. Phys. Chem. 122 (2016) 60.

## Slide 36: Results: Fe
where tbulk is lifetime in non defected structure and m is the trapping coefficient
where: Ssurface - S value for surface, Sbulk- S value for saturation, P(x,E) – implantation profile, L+ - positron diffusion length, a- the positron absorption coefficient at the surface, bulk - the annihilation rate, x - depth
Defect concentration
*) P. Horodek, et al., Rad. Phys. Chem. 122 (2016) 60.

## Slide 37: Results: Fe
Dis
V15
V27
Mean positron lifetime
*) P. Horodek, et al., Rad. Phys. Chem. 122 (2016) 60.

## Slide 38: Results: Cu
*) P. Horodek et al., Vacuum 138 (2017) 15–21.

## Slide 39: Results: Cu
*) P. Horodek et al., Vacuum 138 (2017) 15–21.

## Slide 40: Results: Cu
*) P. Horodek et al., Vacuum 138 (2017) 15–21.

## Slide 41: Results: Cu
Dis
*) P. Horodek et al., Vacuum 138 (2017) 15–21.

## Slide 42: Results: Ag

## Slide 43: Results: Ag
*) J. Dryzek, et al. Acta Pchys. Polon. A 132, 1585 (2017).

## Slide 44: Results: Ag
V+Dis
*) J. Dryzek, et al Acta Pchys. Polon. A 132, 1585 (2017).

## Slide 45: Results: Ti
*)P. Horodek, et al Surf. Coat. Technol. 355, 2018, 247.

## Slide 46: Results: Ti
Dis
V6
*)P. Horodek, et al. Surf. Coat. Technol. 355, 2018, 247.

## Slide 47: Results: Ti
*)P. Horodek et al Surf. Coat. Technol. 355, 2018, 247.

## Slide 48: Results: Bi
*)J.Dryzek, K.Siemek. Appl Phys A 125 2019 85

## Slide 49: Results: Bi
*)J.Dryzek, K.Siemek. Appl Phys A 125 2019 85

## Slide 50: Results
PAS is the sensitive method for detection the structural defects
in dependency on used PAS technique the evaluation of defect profile, approximation of defect concentration or determination of type of defect is possible
the modern application of PAS focuses around slow positron beam studies
PAS studies of irradiated various metals exposed to 167 MeV Xe26+ ions were reported. The aim of investigations was observation of the so called “the long range effect”. This was observed in Fe and Bi samples where defected zone was twice as deep as the implanted depth. In Cu and Ti defects introduced by irradiation occupied theoretically predicted depths

## Slide 51
Thank you for attention!