## Slide 1: LOW-THRESHOLD FIELD ELECTRON EMISSION FROM CARBON NANOCLUSTERS
Georgiy Fursey
Low-dimensional materials: theory, modeling, experiment
Surface Physics and Electronic Research Center RAN
Saint-Petersburg State University
of Telecommunications
Dubna, 9-12 July 2018

## Slide 2: Persons
Bagraev N.T.
Polyakov M.A.
Zakirov I.I.
Voznyakovskii A.P.
Nashchekin A.V.
Bocharov V.N

## Slide 3: Content
Low-Threshold FE
Total energy distribution
Exfoliation of Graphite
High-current emission
About the mechanism

## Slide 4: Low-Threshold Field Emission
Tradition FE 107 V/cm
metals, semiconductors
Low-Threshold FE 104 V/cm
carbon nanostructures
(threshold emission current I0 = 5nA)

## Slide 5: Experiments
Flat
Smooth
Big
surface

## Slide 6: Field emitter
Flat, smooth big surface (dcath= 5-10 mm)
Vacuum gap 2-100 mm
GLS DS, HOPG, CNT, 2D GLS
Constriction of the cathode
Carbon
HOPG

## Slide 7: Surface fragments
F=βU (ϕ = 4,5 eV) need β ~ 104
Big β is unreal!

## Slide 8: Pulse and FE studies
Experimental camera
1. High-voltage input; 2. Cathode; 3. Anode grid; 4,5. Vacuum pump; 6. Electron collector; 7. Window for the photo; 8. Fluorescent screen.
a
b

## Slide 9: Field emission microscopy
GLS
CNT
HOPG
2D carbon structure

## Slide 10: Multiemitter (flakes) cathode
SEM images

## Slide 11: Current-voltage characteristics
Experimental CVC in the Fowler– Nordheim coordinates.

## Slide 12: Total Energy Distribution (TED)
Fundamental peculiarities:
FWHM broadening
Shift of maximum
Two maxima

## Slide 13: TED studies
a) - experimental layout; b) - view through the observation window. 1 — vacuum chamber, 2 — cathode assembly, 3 — greed, 4 — luminescent screen, 5 — protecting cylinder, 6 — hemispherical collector, Ul — the electrostatic lens voltage, Ua — anode voltage, Uret — retarding voltage.

## Slide 14: TED curves of the FE electrons
FWHM broadening 1.5 – 2.5 eV
First maximum shift 1.5 – 3.5 eV below Ef
TED for HOPG
Typical curves of TED
W

## Slide 15: Scheme of low-threshold emission

## Slide 16: High power field emission (“Flash emission”)
Imax ≈ 500 A
Jmax ≈ 50 kA/cm2

## Slide 17: Flash Emission
U
I
1
3
2
τ

## Slide 18: Effect of the Flash Emission
24 kV
80 A
20 ns

## Slide 19: Flash emission from GLS
10 ns
200 A
35 kV
Time sweep is 10 ns per scale mark. Voltage units scale is 17 kV per scale mark. Current units scale is 40 A per scale mark.
The shift of the current pulse reference point with respect to the voltage pulse is an artefact of the recording circuitry parameters adjusting.

## Slide 20: Flash emission from mwCNT
Time sweep is 10 ns per scale mark. Voltage units scale is 17 kV per scale mark. Current units scale is 40 A per scale mark.
10 ns
200 A
44 kV

## Slide 21: Flash emission from HOPG
Pulse Voltage (1) and emission current (2) oscillograms for the HOPG cathode.
Time sweep is 10 ns per scale mark; voltage units scale is 34 kV per 1 V; current units scale is 40 A per 1 V.
440 A
75 kV
10 ns

## Slide 22: “Bilayer” graphene
Material was produced by Voznyakovskii A.P.
Self-propagating high-temperature synthesis method

## Slide 23: Maximum charge as a function of electric field
GLS
CNT
1, 2 - different cathodes
F ∙105 V/cm
F ∙105 V/cm

## Slide 24: FE image of the surface element HOPG
FE image after
a) stationary b) pulse studies
a)
b)

## Slide 25: CVC pulse and stationary
Stationary
Nanosecond pulses

## Slide 26: Emission dependence
C, B – const.
Δ – delta barrier
β – geometrical factor
U - voltage

## Slide 27: Exfoliation of graphite layers in a strong electric field (HOPG, GLS)

## Slide 28: Exfoliation of the surface layers
a1
a3
a2
a1 < a2 < a3
In electric field
Initial state
F1= 0 < F2 < F3

## Slide 29: Exfoliation in a Stationary Electric field (GLS)
a) Initial state b) after the action of field
10 μm
(a)
Fmax ≈ 3 V/μm
(b)
1 μm

## Slide 30: Initial state GLS
10 μm
10 μm

## Slide 31: Exfoliation in a Stationary Electric field (GLS)
10 μm
10 μm
With emission!

## Slide 32: Exfoliation in a Stationary Electric field (HOPG)
a) Initial state b) after the action of field
10 μm
(a)
Fmax ≈ 3 V/μm
With emission!

## Slide 33: Exfoliation in a Stationary Opposite Electric field (HOPG)
a) Initial state b) after the action of field
10 μm
10 μm
Fmax ≈ 3 V/μm
Without emission!

## Slide 34: Exfoliation in a Pulse Direct Electric field
100 nm
Craters
Crater
With emission! I>100 A

## Slide 35: Exfoliation in a Pulse Electric field
Fmax ≈ 30 V/μm
Direct field Opposite field

## Slide 36: Exfoliation in a Pulse Electric field
Direct field Opposite field
1 μm
1 μm
(With emission!) (Without emission!)

## Slide 37: Raman Spectroscopy
Horiba Jobin-Yvon LabRam HR 800
Raman spectrometer
Spectral range: 4000-100 сm-1
Spectral resolution: up to 1.5 сm-1
Lasers:
tunable Ar+ laser with power up to 50mW and with notch filters at 488nm and 514 nm;
He-Ne at 632nm and power up to 10 mW

## Slide 38: Raman spectra after exposure in direct stationary field
after stationary studies
before
2D band
2D
2D
D
G
G

## Slide 39: Raman spectra after exposure in opposite stationary field
after
before
2D band
2D
2D
D
G
G

## Slide 40: Raman spectra after exposure in direct pulse field
after pulse studies
before
2D band
2D
2D
D
G
G

## Slide 41: Raman spectra after exposure in opposite pulse filed
after
before
2D band
2D
2D
D
G
G

## Slide 42: Compare with traditional Raman spectra
A. C. Ferrari, J. C. Meyer, V. Scardaci, et.al., “Raman Spectrum of Graphene and Graphene Layers”, Phys. Rev. Lett., vol. 97, p. 187401, 2006.
With emission
Without emission
Stat.
Pulse
Pulse
Stat.

## Slide 43: ABOUT THE MECHANISM Field emission from carbon structures enhanced by inserting dipole negative-U centers

## Slide 44
The most interstitial- and vacancy-related centers in low-dimensional structures appear to exhibit negative-U properties in the presence of the local vibration mode that gives rise to the spontaneous decay of the one- electron states with the formation of the reconstructed dipole centers.
Specifically, a series of dipole centers that created inside fluted and suspended regions within the preparation of carbon structures seem to result in nanostructures and nanotubes responsible for the spin-dependent quantum transport phenomena.
Moreover, the reconstruction of dipole centers under the application of the external electric field allows the model of the enhanced field emission from carbon-related structures.

## Slide 45
Indeed, the dipole centers appear to result in the surface band bending, with the creation of the deep triangle quantum well and corresponding Femi level pinning varied by the value and the orientation of the external electric field.
Besides, the dipole centers under applied voltage seriously control the characteristics of the delta-barrier that determine the parameters of the electron emission. Thus, the model suggested allows the explanation of the findings of small domains on the emitting surface in which the electric field is able to exceed the value of 108V/cm taking account of the dimensions of dipole structures.
The energy distribution of the emitted carriers reveal the specific maxima the positions of which are in a good agreement with the electron subbands, E1, E2 in the induced quantum well. Finally, this model provides also the quantum effects in the enhanced emission in external magnetic field as well as by varying the value of the longitudinal electric field.

## Slide 46: About the mechanism
Preliminary estimations:
allows to explain 2 peaks in TED
allows to estimate the small effective mass
dipoles give a strong field of 108 V/cm.
That makes the barrier low and very narrow

## Slide 47: Emission process diagram
Vacuum
С
EF
Metal
Evac
E
4,5 eV
1.5 eV
2.5 eV
≈0.01 eV
0

## Slide 48: Conclusions
Direct experiments on large smooth carbon surfaces have established the phenomenon of low-threshold field electron emission. The estimation of the geometrical factor shows that it does not exceed 3-10 times. This allows us to conclude that the phenomenon of LT can not be interpreted from the standpoint of the traditional Fowler-Nordheim theory.
It is established that the spectrum of the emitted electrons is substantially broadened and, unlike metals, has two maxima.
It is found that when an electric field is applied, both direct and opposite sign, the surface layer of the carbon cathode is substantially deformed.
New model for Low-threshold field electron emission is revealed from the experimental data. That is based on the negative-U dipole centers, which are able to create one- and two-dimensional superlattices, with quantum phenomena in the transport processes.
A new effective cathode material from the “bilayer” graphene is proposed.

## Slide 49: Acknowledgements
The author would like to acknowledge
prof. Nikolay Egorov,
prof. Adil Yafyasov,
dr. Vladislav Bojevolnov,

## Slide 50
Cordial thanks to the organizing committee for extraordinary care!!!

## Slide 51: Thank you for the attention!