## Slide 1: ORIGINS OF TERAHERTZ PHOTORESPONSE IN GRAPHENE TRANSISTORS: THEORY AND EXPERIMENT
Gayduchenko I.A.
Dubna, 2018

## Slide 2
1. Introduction:
- What is THz radiation?
- THz Detectors. Why graphene (CNT) based
2. The main mechanisms of THz radiation detection by graphene-based FET devices
3. Asymmetric devices based on graphene:
- Device fabrication and experimental setup
- Device characterization
- Response of asymmetric devices based on graphene on THz radiation
- Contribution of plasmonic response to the detection of sub-terahertz radiation using graphene based devices
4. Conclusions
Graphene based lateral Schottky diodes for detecting terahertz radiation
Outline:

## Slide 3
MOTIVATION

## Slide 4
MOTIVATION
THz range is important for:
Security
Visualization of
the hidden objects

## Slide 5
MOTIVATION
THz range is important for:
Security
Medicine
Visualization of
the hidden objects
THz image of liver

## Slide 6
MOTIVATION
THz range is important for:
Security
Medicine
Astronomy
Etc.
Visualization of
the hidden objects
THz image of liver
Astronomy

## Slide 7
MOTIVATION
Detectors.
Why nanosturtures:
-Sensitive
- Fast
- Energy efficient
- Etc.

## Slide 8
MOTIVATION
Detectors.
Why nanosturtures:
-Sensitive
- Fast
- Energy efficient
- Etc.
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range

## Slide 9
MOTIVATION
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range

## Slide 10
MOTIVATION
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range

## Slide 11
MOTIVATION
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range

## Slide 12
MOTIVATION
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range

## Slide 13
MOTIVATION
Detectors. Why graphene (CNT) based:
Gapless graphene has strong interband absorption at all frequencies
High room-temperature mobility
Geometric control of the band structure
Easy to fabricate
The frequency of graphene plasma waves lies in the terahertz range
Plasmonics forms a major part of the fascinating field of nanophotonics, which explores how electromagnetic fields can be confined over dimensions on the order of or smaller than the wavelength.
Plasmonics: Fundamentals and Applications
Authors: Maier, Stefan Alexander
Springer, 2007

## Slide 14
Study of detection mechanisms
is the study of nonlinearities
What do we mean by graphene THz detector

## Slide 15
Current due to built-in field at the junction OR
rectification due to diode nonlinearity
Voltage due to temperature gradients in nonuniformly doped channel
Resistance change due to
overall device heating
Formation of standing plasma waves in the device channel
Figure from: F.H.L. Koppens, T. Mueller, P. Avouris, A.C. Ferrari, M.S. Vitiello, M. Polini, “Photodetectors based on graphene, other two-dimensional materials and hybrid systems” Nature nanotechnology, 9, 780-793 (2014)
The main mechanisms of THz radiation detection by graphene-based FET devices

## Slide 16
Two types of asymmetric graphene based structures
Asymmetric metallization
Dyakonov – Shur configuration
Difference in workfunction results in formation of a p-n junction along the channel. Schottky diode
Asymmetric boundary conditions:
VS = V0 cos(ωt); ID = 0
Result in a DC voltage signal as the device is exposed to radiation

## Slide 17
*Nature Nanotechnology 9, 814–819 (2014)
Graphene photothermoelectric detector.
Principle of operation
Photo-thermoelectric effect in graphene
Graphene photothermoelectric detector device fabrication and principle of operation. (a-e) Lithographic sequence used to produce the graphene terahertz detector.(f) Optical micrograph showing electrical contacts and (inset) atomic force micrograph showing bimetallic contacts connected to an exfoliated graphene layer. (g-k) Schematic of the principle components during device operation. (g) Cross-sectional view of the device. (h-j) Profiles across the device of (h) electron temperature T(x), (i) Fermi level EF(x), (j) Seebeck coefficient S(x) and (k) potential gradient
Broadband thermoelectric responsivity of graphene photothermoelectric detector. (a,d) Electrical conductance, (b,e) responsivity to Joule heating, and (c,f) responsivity to radiation as a function of gate voltage for the device shown in Fig. 1f at room temperature and in ambient environment.
10 V W–1 (700 V W–1)
Responsivity
Au
Cr

## Slide 18
Detection, mixing, and frequency multiplication of terahertz radiation by two-dimensional electronic fluid*
The basic equations describing the two dimensional electronic fluid are the relationship between the surface carrier concentration and gate voltage swing, the
equation of motion, and the continuity equation
The boundary conditions
*IEEE TRANSACTIONS ON ELECTRON DEVICES, VOL. 43, NO. 3, MARCH 1996

## Slide 19
Detection, mixing, and frequency multiplication of terahertz radiation by two-dimensional electronic fluid
Resonant Detector
ωτ >> 1
Broadband Detector
ωτ <<1
*IEEE TRANSACTIONS ON ELECTRON DEVICES, VOL. 43, NO. 3, MARCH 1996

## Slide 20
NATURE MATERIALS; VOL 11 ;OCTOBER 2012
Due to high room-temperature mobility (up to 10 000 cm2/(V s) on SiO2 graphene is promising for THz FET photodetectors.
Graphene field-effect transistors as room-temperature terahertz detectors*
Diffusive transport model
ωτee <<1
ωτ tr<<1

## Slide 21
NATURE MATERIALS; VOL 11 ;OCTOBER 2012 j
Graphene field-effect transistors as room-temperature terahertz detectors*
The minimum RT NEP is 200nWHz-1/2 for SLG and almost one order of magnitude lower (30nWHz-1/2) for BLG.

## Slide 22
2D FETs for THz detection: Graphene. Further research
Highest mobility devices probed in DS configuration
30µm
D. A. Bandurin, I. Gayduchenko, et al., 112, 141101, (2018)

## Slide 23
2D FETs for THz detection: Graphene. Further research

## Slide 24
2D FETs for THz detection: Graphene. Further research
Evident contact resistance Rc
At least two-fold increase of
Mobility upon cooling
Photo induced voltage
RT mobility

## Slide 25
2D FETs for THz detection: Graphene. Further research
@ Room temperature the response voltage is a linear function of the radiation power
More importantly, R(Vg) follows the F(Vg) with F = dG/dVg * R

## Slide 26
2D FETs for THz detection: Graphene. Further research
At 77 K peak responsivity increases as the radiation power goes down
R(Vg) still follows the F(Vg)

## Slide 27
2D FETs for THz detection: Graphene. Further research
Temperature evolution of responsivity is different for different gate voltages

## Slide 28: Heating-induced photoresponce
Heated region

## Slide 29: Heating-induced photoresponce
Heated region
Temperature evolution of responsivity is different for in case of PURE PTE accounting for the p-n junction at the Ti-Graphene interface (simulations performed by D. Svintsov)
UPTE=(Sch-Scont)(TS-TD)

## Slide 30: Dyakonov-Shur photoresponse

## Slide 31: Conclusions
FET based on graphene encapsulated in hBN can serve as high-responsivity THz detector
Terahertz detection in graphene FETs is a combination of resistive self-mixing, photothermoelectric effects and p-n junction rectification
Hydrodynamics, strong electron-electron and electron-hole scattering are good for photodetection

## Slide 32
I. Gayduchenko, M. Moskotin, N. Titova, B. M. Voronov, N. Kaurova, G. N. Goltsman, MPSU, Moscow, Russia
32
E.D. Obraztsova, M. Rybin, Prokhorov General Physics Institute, Moscow, Russia
G. Fedorov ,D. Svintsov, V G Leiman MIPT, Russia
V. Ryzhii4, , T Otsuji, RIEC, Japan
Collaboration
A. Kuntsevich, CCU, Lebedev Institute
D. Bandurin, The University of Manchester, UK

## Slide 33
I. Gayduchenko, M. Moskotin, N. Titova, B. M. Voronov, N. Kaurova, G. N. Goltsman, MPSU, Moscow, Russia
33
E.D. Obraztsova, M. Rybin, Prokhorov General Physics Institute, Moscow, Russia
G. Fedorov ,D. Svintsov, V G Leiman MIPT, Russia
V. Ryzhii4, , T Otsuji, RIEC, Japan
Collaboration
A. Kuntsevich, CCU, Lebedev Institute
D. Bandurin, The University of Manchester, UK
Thank you for attention!!!