## Slide 1
Structure and properties of aqueous solutions of C60 and C70 fullerenes for biological applications
Olena Kyzyma
Joint Institute for Nuclear Research, Dubna, Russia
Taras Shevchenko Kyiv National University, Kyiv, Ukraine

## Slide 2
Yu.I.Prylutskyy, S.V. Prylutskaya
Biology faculty, Taras Shevchenko Kyiv National University, Ukraine
M.V. Avdeev, O.I. Ivankov, V.L. Aksenov
Frank Laboratory of Neutron Physics, JINR, Dubna, Russia
M.V. Korobov, I.V.Mikheev
Moscow State University, Moscow, Russia
L. Almasy
Wigner Research Center for Physics, Budapest, Hungary
Collaboration
K. Siposova
Institute of Experimental Physics, SAS, Kosice, Slovakia
L.A. Bulavin
Physics faculty, Taras Shevchenko Kyiv National University, Ukraine
V. Haramus
Helmholtz-Zentrum Geesthacht, Germany
S.V. Sarantseva, O.I. Bolshakova
Petersburg Nuclear Physics Institute, NRC KI, Gatchina, Russia
Chemistry
Physics
Biology
I.V. Koshlan, P. Blaha
Laboratory of Radiation Biology, JINR, Dubna, Russia
2

## Slide 3
Outline
Introduction: Fullerenes in solutions
Structure analysis:
      Fullerene water solutions
      Complexes С60 +Drugs (Prodrugs)
Biological properties: Anti-cancer treatments
Prospects: Fullerenes as anti-amyloid agents
3

## Slide 4
Nobel Prize in Chemistry 1996
C60
Diamond
H.W.Kroto
R.F.Curl
R.E.Smalley
D ~ 1 nm
Graphite
Fullerenes – new allotropic state of carbon
4

## Slide 5
Mainly molecular solutions
Low-polar solvents
(toluene, benzene)
(ε< 10)
Solubility up 50 mg/ml
Polar solvents
(pyridine, N-methylpyrrolidone)
( > 10)
Solubility up 1 mg/ml
Non-soluble in water!!!!
Cluster formation after dissolution
D = 1 nm
D < 500 nm
M.V.Avdeev, T.V.Tropin, V.L.Aksenov, “Models of cluster formation of fullerenes in solutions”
Rus. J. Phys. Chem. A (2010)
Highly polar solvents
(alcohol, water)
( = 82)
H2O
Fullerenes in solutions and cluster formation
5

## Slide 6
Fullerenes water solutions
G.V.Andrievsky, et al. J. Chem. Soc., Chem. Commun. 1995
Via Solubilization
Guldi, D. M. et al. J. Phys. Chem. (1995) 9380
Modified fullerene
water dispersions
With the Help of Covalent Modifications
Solvent exchange method
C60-toluene
Fullerene
Water
solution
H2O
ultrasound
D ~ 100 nm
Stable colloidal (cluster) solutions with electrostatic stabilization
Wide prospects for biomedical applications
FASnC60
Non-modified fullerene
water dispersions
FASnC70
Reduction in aggregate size is required
6

## Slide 7
Fullerene water solution NMP/nC60
Dilution of C60/NMP system with water leads to the decomposition of clusters in solutions. It is possible to regulate the size of fullerene aggregates in water!
Cluster reorganization in C60/NMP solution at water addition.
Fullerene water solution NMP/nC60
O.A. Kyzyma, T.О. Kyrey, M.V. Avdeev et al. Chem. Phys. Lett. 556(2013)178
T.O. Kyrey, O.A. Kyzyma, M.V. Avdeev et al. Fullerenes Nanotubes Carbon Nanostruc. 20(2012)341
unaged
С60/N-methylpirrolidon (NMP)
SANS
aged C60/NMP
+Н20
time
D ~ 100 nm
D < 30 nm
DLS
NMP < 0,005 vol.%
D ~5 nm
+Н20
C60
C60 −NMP complex
NMP
7

## Slide 8
Fullerene water solution NMP/nC60
Dilution of C60/NMP system with water leads to the decomposition of clusters in solutions. It is possible to regulate the size of fullerenes aggregates in water!
Cluster reorganization in C60/NMP solution at water addition.
Preparation of fullerene water solution NMP/nC60
O.A. Kyzyma, T.О. Kyrey, M.V. Avdeev et al. Chem. Phys. Lett. 556(2013)178
T.O. Kyrey, O.A. Kyzyma, M.V. Avdeev et al. Fullerenes Nanotubes Carbon Nanostruc. 20(2012)341
unaged
С60/N-methylpirrolidon (NMP)
SANS
aged C60/NMP
+Н20
time
D ~ 100 nm
D < 30 nm
DLS
NMP < 0,005 vol.%
D ~5 nm
+Н20
C60
C60 −NMP complex
NMP
      Method of regulation of the fullerene aggregates size in water was developed.
      Fullerene water solutions with small aggregate size (< 30 nm) were obtained.
7

## Slide 9
D ≤ 150 nm
DLS
Son/n C60
IR
D < 30 nm
AFM
Son/n C70
toluene
H2O
ultrasound
NMP/nC60
H2O
NMP< 0.005 Vol.%
NMP
AFM
NMP/nC70
In physiological solution
NaCl
Structure of fullerene water solutions
Y. Prylutskyy, V. Petrenko, O. Ivankov, O. Kyzyma, et al. Langmuir 30 (2014)3967.
8
SAXS/SANS

## Slide 10
D ≤ 150 nm
DLS
Son/n C60
IR
D < 30 nm
AFM
Son/n C70
toluene
H2O
ultrasound
NMP/nC60
H2O
NMP< 0.005 Vol.%
NMP
AFM
NMP/nC70
In physiological solution
NaCl
Structure of fullerene water solutions
Y. Prylutskyy, V. Petrenko, O. Ivankov, O. Kyzyma, et al. Langmuir 30 (2014)3967.
      The cluster formation under various conditions (temperature, ionic strength, pH) in aqueous colloidal solutions of fullerenes were described in detail.
      Cluster stabilization mechanism was identified.
8

## Slide 11
Fullerene-based antitumor complexes
H6Cl2N2Pt
Cisplatin
C60+LA
Son/nC60
31 нм
21 нм
Landomycin A
ICR-191
Yu.I. Prylutskyy, V.V. Cherepanov, V.V. Kostjukov, O.A. Kyzyma, et al. RSC Advаnces 6(2016)81231
A. Borowik, Yu. Prylutskyy, Ł. Kawelski, O. Kyzyma, et al. Colloids and Surfaces B 164 (2018)134
Yu.I. Prylutskyy, V.V. Cherepanov, M.P. Evstigneev, O.A. Kyzyma, et al. Phys. Chem. Chem. Phys. 17(2015)26084
S. Prylutska, R. Panchuk, G. Gołuński, O. Kyzyma, et al.
Nano Res. 10(2017)652
C60+LA
Son/nC60
9

## Slide 12
Fullerene-based antitumor complexes
H6Cl2N2Pt
Cisplatin
C60+LA
Son/nC60
31 нм
21 нм
Landomycin A
ICR-191
Yu.I. Prylutskyy, V.V. Cherepanov, V.V. Kostjukov, O.A. Kyzyma, et al. RSC Advаnces 6(2016)81231
A. Borowik, Yu. Prylutskyy, Ł. Kawelski, O. Kyzyma, et al. Colloids and Surfaces B 164 (2018)134
Yu.I. Prylutskyy, V.V. Cherepanov, M.P. Evstigneev, O.A. Kyzyma, et al. Phys. Chem. Chem. Phys. 17(2015)26084
S. Prylutska, R. Panchuk, G. Gołuński, O. Kyzyma, et al.
Nano Res. 10(2017)652
      For all mixtures the formation of stable complexes were proved.
The complexation leads to significant changes in the cluster state of the initial fullerene solutions.
9

## Slide 13
Survival rate > 80% in all samples!
Chinese-hamster V-79 cells
Cells growth period 13 days
Fullerene concentration range 0.05–5 μg/mL
NMP/nC60
D~30 nm
son/nС60
D~90 nm
son/nC70
D~130 nm
In vitro investigation: cytotoxicity
E. A. Kyzyma, A. A. Tomchuk, L. A. Bulavin, et al. J. Surf. Invest.9(2015) 5
Chart: Period of growth (days)
| 4 | 7 | 9 | 11 | 13
0.05 μg/ml | 0.93633 | 0.975 | 0.98 | 0.94 | 0.88
0.5 μg/ml | 0.85 | 0.955 | 0.92 | 0.92
5 μg/ml | 0.848 | 0.955 | 0.99 | 0.85
Control | 0.92 | 0.967 | 0.92
Chart: Period of growth (days)
| 4 | 7 | 9 | 13
0.05 μg/ml | 0.93 | 0.975 | 0.97 | 0.9
0.5 μg/ml | 0.95 | 0.975 | 0.93 | 0.72
5 μg/ml | 0.7725 | 0.963 | 0.96 | 0.96
Control | 0.92 | 0.967 | 0.92
Chart: Period of growth (days)
| 4 | 7 | 9 | 11
0.05 μg/ml | 0.9 | 0.97 | 0.92 | 0.9
Control | 0.92 | 0.967 | 0.92
10

## Slide 14
Survival rate > 80% in all samples!
Chinese-hamster V-79 cells
Cells growth period 13 days
Fullerene concentration range 0.05–5 μg/mL
NMP/nC60
D~30 nm
son/nС60
D~90 nm
son/nC70
D~130 nm
In vitro investigation: cytotoxicity
E. A. Kyzyma, A. A. Tomchuk, L. A. Bulavin, et al. J. Surf. Invest.9(2015) 5
Chart: Period of growth (days)
| 4 | 7 | 9 | 11 | 13
0.05 μg/ml | 0.93633 | 0.975 | 0.98 | 0.94 | 0.88
0.5 μg/ml | 0.85 | 0.955 | 0.92 | 0.92
5 μg/ml | 0.848 | 0.955 | 0.99 | 0.85
Control | 0.92 | 0.967 | 0.92
Chart: Period of growth (days)
| 4 | 7 | 9 | 13
0.05 μg/ml | 0.93 | 0.975 | 0.97 | 0.9
0.5 μg/ml | 0.95 | 0.975 | 0.93 | 0.72
5 μg/ml | 0.7725 | 0.963 | 0.96 | 0.96
Control | 0.92 | 0.967 | 0.92
Chart: Period of growth (days)
| 4 | 7 | 9 | 11
0.05 μg/ml | 0.9 | 0.97 | 0.92 | 0.9
Control | 0.92 | 0.967 | 0.92
      Low toxicity of all fullerene solutions under study was detected.
Cluster growth does not impair the toxicity of the solutions.
10

## Slide 15
Son/nС60
Dox
Son/nС60+Dox
15%
23%
35%
Lifespan
Tumor-inhibitory effect
24%
16%
32%
Visual observation of Lewis lung carcinoma growth in mice.
Control -a), injections son/nC60 - b), injections Dox - c) injections son/nC60+Dox - d) 20 days after tumor transplantation.
The male mice of С57Bl/6J line (20–21 g weight)
Biological effect
Control
Son/nC60
Dox
Son/nC60 +Dox
Son/nC60
Dox
Son/nC60 +Dox
Growth inhibition curves for treatment of tumor-bearing animals with C60 fullerene, doxorubicin, or C60+ doxorubicin (p<0.05) ).
It was found that treatment of tumor by Dox with C60 fullerene leads to increase enhancement of antitumor action of Dox, by compare such effect when the drug is used alone.
S. Prylutska et al. Drugs R D (2014)14, p.333
Panchuk et al. J. Biomed. Nanotechnol(2015)11,1139–1152
11

## Slide 16
Son/nС60
Dox
Son/nС60+Dox
15%
23%
35%
Lifespan
Tumor-inhibitory effect
24%
16%
32%
Visual observation of Lewis lung carcinoma growth in mice.
Control -a), injections son/nC60 - b), injections Dox - c) injections son/nC60+Dox - d) 20 days after tumor transplantation.
The male mice of С57Bl/6J line (20–21 g weight)
Biological effect
Control
Son/nC60
Dox
Son/nC60 +Dox
Son/nC60
Dox
Son/nC60 +Dox
Growth inhibition curves for treatment of tumor-bearing animals with C60 fullerene, doxorubicin, or C60+ doxorubicin (p<0.05) ).
It was found that treatment of tumor by Dox with C60 fullerene leads to increase enhancement of antitumor action of Dox, by compare such effect when the drug is used alone.
S. Prylutska et al. Drugs R D (2014)14, p.333
Panchuk et al. J. Biomed. Nanotechnol(2015)11,1139–1152
      It was found that prodrugs (complex) in a low therapeutic dose enhance the inhibition of tumor growth and lifespan to much higher extent than antibiotic alone
11

## Slide 17
Neurodegenerative diseases are caused by deposition of amyloid fibrils in the organs and tissues in the body
Fullerenes in therapy of neurodegenerative diseases
Advanced
Alzheimer's
Healthy brain
promote and enhance the rate of amyloid fibril formation
copolymer, cerium oxide, TiO2 nanoparticles, carbon nanotubes
(Linse S et al., Proc. Natl. Acad. Sci. 2007,
Wu et al. Biochem. Biophys. Res. Commun, 2008)
no potential to induce protein amyloid aggregation
negatively charged silica nanoparticles
(Wu et al. Biochem. Biophys. Res. Commun, 2008)
Destruction/depolymerization
magnetic nanoparticles
(Skaat H, et al. J. Biomed.Mater. Res. 2008,
Siposova K. , et al. Nanotechnology 2012)
Impact of nanoparticles on amyloids:
12

## Slide 18
Impact of NMP/nC60 on Insulin fibrils
ThT assay
+ NMP/nC60
Insulin
10:1
2:1
DEPOLYMERIZATION EFFECT
NMP/nC60
NMP
depolymerization
inhibition
NMP/nC60, mg ml-1
13

## Slide 19
Impact of NMP/nC60 on Insulin fibrils
ThT assay
+ NMP/nC60
Insulin
10:1
2:1
DEPOLYMERIZATION EFFECT
NMP/nC60
NMP
depolymerization
inhibition
      Fullerene solution inhibit formation of insulin fibrils and destroy amyloid aggregates.
      Pure NMP has no effect on amyloid aggregates.
13

## Slide 20
The cluster formation under various conditions (temperature, ionic strength, pH) in aqueous colloidal solutions of fullerenes are described in detail.
As a result, new stable fullerene water solutions, NMP/nC60 and NMP/nC70, with small aggregate size and low toxicity were synthesized.
The found complexation of fullerenes with antitumor drugs, as well as destroying effects on amyloid fibrils indicate that fullerenes are promising antitumor and anti-amyloid agents.
Conclusions
~80-100 nm
~0,7 nm
0
~30 nm
20
40
60
80
nmp/nC60,70
100 nm
Solutions by commonly
used technique
New technique
son/nC60,70

## Slide 21
Thank you for your attention!