## Slide 1: The abnormal behavior of the resistive transition to the normal state of superconducting high-textured Nb-Ti tapes just below Hc2
Valentin Guryev, Sergey Shavkin, Vitaliy Kruglov
NRC “Kurchatov institute”
2018
The XXII International Scientific Conference of Young Scientists and Specialists (AYSS-2018)

## Slide 2
Introduction
Temperature phase transition
Field phase transition
Current phase transition
?

## Slide 3
Object of study
Cold rolled single-phase β-Nb-Ti tape of Nb-50 mass% Ti alloy
The well-developed technology for manufacturing Nb-Ti superconductors can guarantee the homogeneity of the tape, which ensures the reproducibility of the results of experimental studies, allowing to study physical patterns, rather than individual features of specific samples.
A pure superconductor is in the place of the measuring bridge. There are no shunting layers of copper.

## Slide 4
Critical current vs magnetic field

## Slide 5
Current-Voltage Characteristic at high magnetic field
?

## Slide 6
Hysteresis of the Current-Voltage Characteristics
RN

## Slide 7
From CVC to Current-Resistivity Characteristics
step 0.2 T
step 0.2 T

## Slide 8
1
2
3
4
Common features of hysteresis of the Current-Resistivity Characteristics

## Slide 9
Interpretation
The same behavior was observed on granular superconductors*.
*-Turutanov O.G. ”Abnormal (non-thermal) hysteresis at current-voltage characteristics of granulated vanadium thin films in magnetic fields” // Bul.Zap.Nat.Uni. (2015) №3
rolling direction
<l>=3 μm
<d>=65 nm

## Slide 10
Conclusions
            1) The abnormal hysteresis of the current-voltage characteristics was detected in high magnetic fields (just below Hc2) on Nb-Ti tapes.
            2) An interpretation of this hysteresis is proposed in the framework of the granular superconductor model. This model is an alternative to the widespread idea of a phase transition in the vortex matter.
            3) This interpretation is in good agreement with the experimental data obtained in our group earlier

## Slide 11
Thank you for attention!

## Slide 12
?
Giant Flux Creep
Phase transition in the vortex matter
Thermal fluctuations