## Slide 1: Magnetic phenomena in cobalt intermetallides at high pressures
A.V. Rutkauskas, D. P. Kozlenko, N.O. Golosova,
S.E. Kichanov, B.N.Savenko,
E. Burzo, P. Vlaic

## Slide 2
The intermetallic compounds R-Co
Strong correlated systems:
charge, structural, spin
Giant magnetoresistance effects
Magnetocaloric effects
Magnetoelastic effects
Structural phase transitions
Magnetic phase transitions
Technological applications
Permanent magnets
Magnetocaloric devices
Magnetoresistive data storage and recording
Physical phenomena
2

## Slide 3
Magnetic phenomena
Non-magnetic R-ions:
YCo2 or LuCo2
MR = 0 μB
MCo = 0 μB
Paramagnetic state
up to 70-75 T
Magnetic R-ions:
TbCo2, HoCo2,
ErCo2, DyCo2
MR = 6-10 μB
MCo = ~1 μB
R
R
Co
Phys. Rev. B 57, 2904 (1998).
3
YCo5-xMx (M = Si, B)
Romanian Reports in Physics, Vol. 64, Supplement, P. 1195–1206, 2012

## Slide 4
DN-12 diffractometer for studies of microsamples (~ 1 mm3)
High pressure techniques on the IBR-2 reactor
DN-6 diffractometer for high pressure studies (~ 0.001 mm3)
Maximum pressure is 8 GPa =80 000 atm
Maximum pressure is 40 GPa =400 000 atm
4

## Slide 5
Magnetic phenomena of TbCo2
The rhombohedral symmetry Rm at T < 230 K
Neutron diffraction patterns of TbCo2, measured at different pressures and temperatures
5
Pressure dependencies of nearest-neighbor
Co-Co distances
dT/dP = -9 K/GPa
Temperature dependencies of Tb and Co
ordered magnetic moments at selected pressures

## Slide 6
Magnetic phenomena of DyCo2
Pressure dependencies of lattice parameters
and nearest-neighbor Co-Co distances in DyCo2
dT/dP = -4.6 K/GPa
Temperature dependencies of Dy and Co ordered
magnetic moments at selected pressures
Neutron diffraction patterns of DyCo2, measured at different pressures and temperatures.
The tetragonal structure
I41/amd at T ˂ 145 K
6

## Slide 7
Magnetic phenomena of HoCo2
The tetragonal structure I41/amd при T ˂ 78 K
Neutron diffraction patterns of HoCo2,
measured at different pressure and temperature.
7
Temperature dependencies of Ho and Co ordered
magnetic moments at selected pressures
Pressure dependencies of lattice parameters
and nearest-neighbor Co-Co distances in HoCo2

## Slide 8
The rhombohedral structure
Rm at T < 36 K
Magnetic phenomena of ErCo2
8
dTС (Co)/ dP = - 4(1) K/ГПа
Neutron diffraction patterns of ErCo2,
measured at different pressures and temperatures.
Temperature dependencies
of Er and Co ordered magnetic moments at selected pressures
Pressure dependencies of lattice parameters
and nearest-neighbor Co-Co distances in HoCo2

## Slide 9
Magnetic phenomena of YCo5
Neutron diffraction patterns of YCo5 at selected pressures, processed by the Rietveld method.
P = 0 GPa (v/v0 = 1)
P ≥ 4.5 Gpa
(v/v0 ≤ 0.956)
Pressure dependences of lattice parameters and the c/a ratio (inset).
P = 7.2 Gpa
(v/v0 ) 0.924)
9

## Slide 10
Neutron diffraction patterns of YCo5 at selected pressures, processed by the Rietveld method.
P = 3,5 GPa
(v/v0 = 0,97)
P = 5,3GPa
(v/v0 = 0,95)
P = 0 GPa
(v/v0 = 1)
MCo(2c) = 1,03 µB
MCo(3g) = 1,39 µB
MCo(2c) = 0,96 µB
MCo(3g) = 1,25 µB
MCo(2c) = 0,90 µB
MCo(3g) = 1,1 µB
Magnetic phenomena of YCo4Si
10

## Slide 11
Summary
In RCo2 (R – Tb, Ho, Dy) the rare-earth and cobalt sublattices behave as agreed under pressure and have the same Curie temperatures
In ErCo2 disagreed behavior of the magnetic ordering in the cobalt and erbium sub-lattices caused by pressure is observed. It related with a strong anisotropy in baric changes in interatomic bonding.
In YCo5 lattice collapse is detected
In YCo4Si the point of volume collapse and suppression of the magnetic structure is reached

## Slide 12
Thank you for your attention!